Supporting Information

Ultra-Narrow Pure-Green MR-TADF Emitter with an FWHM of 12 nm Enables Superior-Performance Top-Emitting OLEDs with EQE Approaching 60%, Power Efficiency over 300 lm W-1, and CIE Coordinates of (0.14, 0.79)

Zhuixing Xue, Yuxuan Hu*, Jiahui Liu, Sijie Xian, Shengbing Xiao, Zeyuan Ye, Zhiyi Chen, Xiudan Zhang, Jingsheng Miao, and Chuluo Yang*

Shenzhen Key Laboratory of New Information Display and Storage Materials, College of Materials Science and Engineering, Shenzhen University, Shenzhen, 518060 (P. R. China)

Corresponding Authors

Yuxuan Hu, Email: huyuxuan@szu.edu.cn

Chuluo Yang, Email: clyang@szu.edu.cn

Table of Contents

- Experimental sectionS3

1.1 Materials and MethodsS3

1.2 SynthesisS3

1.3 Single Crystal X-ray CrystallographyS7

1.4 Thermal and Electrochemical characterizationS7

1.5 Photophysical characterizationS8

1.6 Quantum chemical calculationsS8

1.7 Analysis of rate constantsS8

1.8 Device Fabrication and MeasurementS9

2. Figures and TablesS10

3. ReferencesS37

- Experimental section

## 1.1 Materials and Methods

All reagents were used as received from commercial sources without further purification unless otherwise mentioned. Solvents for chemical synthesis were purified according to the standard procedures. All reactions were heated by metal sand bath (WATTCAS, LAB-500, https://www.wattcas.com). NMR spectra were measured on Bruker Advance spectrometers (400 MHz and 500 MHz for 1H NMR, and 126 MHz for 13C NMR). Tetramethylsilane was used as the internal standard and CD2Cl2, DMSO-d6 and CDCl3 as the solvents. The high-resolution mass spectrometry (HR-MS) for the compounds was conducted on a Thermo Scientific LTQ Orbitrap XL with ESI ion source.

## 1.2 Synthesis

Scheme S1. Synthetic route of DBN.

Synthesis of 1: Under argon atmosphere, a mixture of compound 1,3-dibromo-5-chlorobenzene (8.00 g, 29.59 mmol), 2,6-dimethylaniline (8.25 g, 68.06 mmol), Pd2(dba)3 (217 mg, 0.24 mmol), S-Phos (850 mg, 2.07 mmol) and tBuONa (9.95 g, 103.56 mmol) in 120 mL deoxygenated solution (xylenes) was stirred at 100 °C for 8 h under an argon atmosphere. After cooling to room temperature, the reaction mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 4:1, ν/ν), giving the intermediate 1 as a white solid (7.37 g, yield 71%). 1H NMR (400 MHz, CDCl3) δ (ppm): 7.15 – 7.03 (m, 6H), 5.85 (s, 1H), 5.84 (s, 1H), 5.56 (t, J = 2.0 Hz, 1H), 5.06 (s, 2H), 2.21 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 148.48, 137.75, 136.32, 135.86, 128.63, 126.23, 103.91, 96.69, 18.41.

Synthesis of 2: Under argon atmosphere, intermediate 1 (5.00 g, 14.25 mmol), bromobenzene (1.72 g, 10.96 mmol), Pd2(dba)3 (151 mg, 0.16 mmol), DPPF (197 mg, 0.88 mmol) and tBuONa (2.11 g, 21.92 mmol) were added into a 200 mL two-neck flask. Then, 350 mL deoxygenated solution (xylenes) was injected into the mixture. The reaction was refluxed for 8 h at 100 ºC. After cooling to room temperature, the reaction mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 4:1, ν/ν), giving the intermediate 2 as a white solid (5.70 g, yield 52%). 1H NMR (500 MHz, DMSO-d6) δ (ppm): 7.24 – 7.20 (m, 2H), 7.19 – 7.14 (m, 3H), 7.07 – 6.99 (m, 3H), 6.91 (d, J = 7.3 Hz, 1H), 6.88 (s, 2H), 5.98 (s, 1H), 5.95 (t, J = 2.0 Hz, 1H), 5.87 (s, 1H), 2.09 (s, 6H), 1.96 (s, 6H). 13C NMR (126 MHz, CDCl3) δ (ppm): 148.27, 148.10, 145.30, 142.41, 137.95, 137.49, 136.11, 135.58, 129.24, 129.06, 128.55, 127.28, 126.22, 121.50, 120.76, 109.25, 105.70, 102.50, 18.64, 18.28.

Synthesis of 3: Under argon atmosphere, intermediate 2 (3.80 g, 8.91 mmol), 1,3-dibromobenzene (0.95 g, 4.05 mmol), Pd2(dba)3 (75 mg, 0.08 mmol), S-Phos (134 mg, 0.32 mmol) and tBuONa (1.55 g, 16.21 mmol) were added into a 100 mL two-neck flask. Subsequently, 20 mL deoxygenated solution (xylenes) was injected into the mixture, which was refluxed for 10 h at 120ºC. After cooling to room temperature, the mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed under reduced pressure, then the crude product was purified by silica gel column chromatography (eluent: petroleum ether/dichloromethane = 4:1, ν/ν), giving the intermediate 3 as a white solid (2.71 g, yield 72%). 1H NMR (500 MHz, CDCl3) δ (ppm): 7.15 – 7.07 (m, 6H), 7.06 – 6.98 (m, 6H), 6.98 – 6.90 (m, 5H), 6.85 (d, J = 7.7 Hz, 6H), 6.52 (dd, J = 8.1, 2.2 Hz, 2H), 6.39 (s, 2H), 6.35 (s, 2H), 6.27 (s, 2H), 6.22 (s, 1H), 1.94 (s, 12H), 1.87 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 147.53, 147.34, 145.89, 145.09, 142.05, 141.91, 137.71, 137.34, 135.26, 129.26, 129.20, 129.02, 127.32, 127.18, 121.31, 119.97, 113.19, 112.17, 111.55, 111.47, 108.48, 18.46, 18.27.

Synthesis of DBNCl: In a 200 mL sealed tube charged with argon, a solution of intermediate 3 (2.3 g, 2.48 mmol) in 15 ml of highly dry 1,2-dichlorobenzene was prepared. After boron tribromide (14.0 equiv.) was added, the tube was sealed and then the reaction was heated and stirred at 200ºC for 36 h. Upon cooling to ambient temperature, the reaction was quenched by the dropwise addition of ethanol (15.0 mL) under an ice bath. The accumulated organic solvent was concentrated in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 4:1, ν/ν), yielding the intermediate DBNCl (1.59 g, 68% yield) as yellow solids. 1H NMR (500 MHz, CDCl3) δ (ppm): 10.70 (s, 1H), 9.33 (d, J = 7.4 Hz, 2H), 7.52 (t, J = 7.7 Hz, 2H), 7.43 (d, J = 7.4 Hz, 4H), 7.36 (d, J = 7.5 Hz, 4H), 7.21 (t, J = 7.7 Hz, 2H), 7.08 (d, J = 7.6 Hz, 4H), 6.73 (d, J = 8.6 Hz, 2H), 6.24 (d, J = 9.3 Hz, 4H), 5.67 (s, 1H), 1.95 (s, 12H), 1.81 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 148.53, 146.32, 146.08, 145.64, 144.66, 138.93, 138.39, 137.61, 136.85, 135.55, 131.89, 129.83, 129.43, 128.94, 128.67, 128.25, 120.86, 115.71, 107.18, 106.81, 99.59, 17.62, 17.34.

Synthesis of DBN: Under argon atmosphere, intermediate DBNCl (400 mg, 0.42 mmol), Pd2(dba)3 (12 mg, 0.01 mmol), S-Phos (17 mg, 0.04 mmol) and tBuOK (285 mg, 2.54 mmol) were added into a 100 mL two-neck flask. Subsequently, deoxygenated EtOH (117 mg, 2.54 mmol) and 15 mL deoxygenated solution (xylenes) were injected into the mixture, which was refluxed for 1 h at 120 ºC. After cooling to room temperature, the mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed under reduced pressure, then the crude product was purified by silica gel column chromatography (eluent: petroleum ether/dichloromethane = 3:1, ν/ν), giving the intermediate DBN as a yellow solid (254 mg, yield 69%). 1H NMR (500 MHz, CD2Cl2) δ (ppm): 10.70 (s, 1H), 9.34 (d, J = 7.9 Hz, 2H), 7.53 (t, J = 7.0 Hz, 2H), 7.47 – 7.33 (m, 8H), 7.27 (t, J = 8.3 Hz, 2H), 7.22 (t, J = 7.6 Hz, 2H), 7.11 – 7.09 (m, 4H), 6.76 (d, J = 8.3 Hz, 2H), 6.10 (s, 4H), 5.71 (s, 1H), 1.93 (s, 12H), 1.80 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 148.69, 145.86, 145.41, 145.19, 144.77, 139.65, 139.16, 137.94, 137.17, 135.74, 133.05, 131.58, 129.60, 129.16, 128.54, 128.23, 124.77, 120.26, 118.83, 117.31, 115.43, 104.20, 103.78, 98.96, 17.66, 17.39.

Scheme S2. Synthetic route of DBFBN and DBFCN.

Synthesis of DBFBN: Under argon atmosphere, intermediate DBFCl (350 mg, 0.31 mmol), Pd2(dba)3 (14 mg, 0.02 mmol), S-Phos (13 mg, 0.03 mmol) and tBuOK (209 mg, 1.87 mmol) were added into a 100 mL two-neck flask. Subsequently, deoxygenated EtOH (86 mg, 1.87 mmol) and 15 mL deoxygenated solution (xylenes) were injected into the mixture, which was refluxed for 1 h at 120 ºC. After cooling to room temperature, the mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed under reduced pressure, then the crude product was purified by silica gel column chromatography (eluent: petroleum ether/dichloromethane = 5:2, ν/ν), giving the intermediate DBFBN as a yellow solid (233 mg, yield 71%). 1H NMR (500 MHz, CDCl3) δ (ppm): 10.90 (s, 1H), 9.61 (s, 2H), 7.89 (d, J = 7.6 Hz, 2H), 7.56 (d, J = 8.1 Hz, 2H), 7.51 (d, J = 7.4 Hz, 2H), 7.49 – 7.45 (m, 2H), 7.43 (d, J = 7.4 Hz, 4H), 7.32 – 7.27 (m, 6H), 7.21 (t, J = 7.7 Hz, 2H), 7.09 (d, J = 7.7 Hz, 4H), 6.12 (t, J = 8.7 Hz, 4H), 5.77 (s, 1H), 2.01 (s, 12H), 1.86 (s, 12H). 13C NMR (101 MHz, CDCl3) δ (ppm): 157.98, 151.92, 148.75, 145.36, 143.84, 142.31, 140.09, 139.12, 138.07, 137.16, 133.16, 129.82, 129.16, 128.66, 128.25, 128.12, 124.59, 122.06, 121.47, 116.30, 111.78, 105.96, 104.08, 103.49, 99.07, 17.72, 17.42. HR-MS (ESI) m/z [M+H]+ calcd for C76H54B2N4O2+ 1055.4589, found 1055.4648.

Synthesis of DBFCN: Under argon atmosphere, intermediate DBFCl (400 mg, 0.36 mmol), Zn(CN)2 (63 mg, 0.53 mmol), Zn (349 mg, 5.34 mmol), Pd2(dba)3 (98 mg, 0.11 mmol), X-Phos (68 mg, 0.14 mmol) and K2CO3 (15 mg, 0.11 mmol) were added into a 100 mL two-neck flask. Then, 15 mL deoxygenated DMF was injected into the mixture. The reaction was refluxed for 20 h at 150 ºC. After cooling to room temperature, the reaction mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 2:1, ν/ν), giving the DBFCN as an orange-yellow solid (220 mg, yield 56%). 1H NMR (500 MHz, CDCl3) δ (ppm): 10.90 (s, 1H), 9.56 (s, 2H), 7.91 (d, J = 7.7 Hz, 2H), 7.60 – 7.51 (m, 6H), 7.47 (d, J = 7.7 Hz, 4H), 7.34 (d, J = 9.5 Hz, 4H), 7.28 (d, J = 7.7 Hz, 2H), 7.14 (d, J = 7.7 Hz, 4H), 6.42 (s, 2H), 6.37 (s, 2H), 5.84 (s, 1H), 1.99 (s, 12H), 1.84 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 158.10, 152.33, 148.78, 145.59, 145.40, 144.34, 142.04, 138.93, 137.92, 137.52, 136.66, 130.30, 129.66, 129.49, 129.10, 129.05, 128.71, 124.18, 122.41, 121.71, 120.08, 116.18, 115.74, 111.84, 107.42, 106.67, 106.15, 99.86, 17.60, 17.30. HR-MS (ESI) m/z [M+H]+ calcd for C76H54B2N6O2+ 1105.4494, found 1105.4547.

## 1.3 Single Crystal X-ray Crystallography

X-ray single crystal data was collected on a Bruker D8 Venture diffractometer using Ga Kα radiation (λ = 1.34139) source. The selected crystal was kept at 170.0 K during data collection. Using Olex21, the structure was solved with the ShelXT2 structure solution program using Intrinsic Phasing and refined with the ShelXL3 refinement package using Least Squares minimization. Selected crystal data are listed in Table S1. All crystallographic information in CIF format has been deposited at the Cambridge Crystallographic Data Center (CCDC) under deposition number of 2542652 for DBFCN via www.ccdc.cam.ac.uk/data_request/cif, or by emailing data_request@ccdc.cam.ac.uk, or by contacting the Cambridge Crystallographic Data Center, 12 Union Road, Cambridge CB2 1EZ, UK; fax: +44 1223 336033.

## 1.4 Thermal and Electrochemical characterization

Thermogravimetric analysis (TGA) was undertaken using TGA-Q50 Instrument (TA Instruments, America) at a heating rate of 10 °C/min from 50 °C to 700 °C under nitrogen flushing. The thermal decomposition temperatures (Td) were determined by the recorded temperature at 5% weight loss. Cyclic voltammetry (CV) measurements were performed on a CH1660E electrochemical workstation using n-Bu4NPF6 (0.1 M) in dichloromethane (DCM) as electrolyte solution and ferrocene as an internal reference at a scan rate of 0.1 V s–1. The CV cell consisted of a glassy carbon electrode, a Pt wire counter electrode, and a standard Ag/AgCl reference electrode. The emitters were spin-coated on the working electrode for measurements. The redox potentials were calibrated with ferrocene as an internal standard. The highest occupied molecular orbital (HOMO) energy levels of the emitters were estimated by the equation: EHOMO = ‒ (4.80 + Eonsetox) eV. The lowest unoccupied molecular orbital (LUMO) energy levels of the emitters were calculated by ELUMO = EHOMO + Eg, and Eg is the optical band gap calculated from the absorption onset in dilute toluene (10-5 M).

## 1.5 Photophysical characterization

The UV-vis absorption spectra were obtained on a Shimadzu UV-2600 spectrophotometer (Shimadzu, Japan) at room temperature with a concentration of 1×10-5 M. Phosphorescence spectra were measured on a Hitachi F-7100 fluorescence spectrophotometer at 77 K. The transient photoluminescence (PL) decay curves were obtained by FluoTime 300 (PicoQuant GmbH) with a Picosecond Pulsed UV-LASTER (LASTER375) as the excitation source. The solid-state PL quantum efficiencies (ΦPLs) were measured on a Hamamatsu UV-NIR absolute PL quantum yield spectrometer (C13534, Hamamatsu Photonics) equipped with an integrating sphere.

## 1.6 Quantum chemical calculations

All of the calculations were carried out with Gaussian 09 program package.[1] Density functional theory (DFT) calculations on the geometrical and electronic properties of the ground-state were performed based on B3LYP[2] density functional method with basis set 6-31G(d,p).[3,4] The density functional dispersion correction was conducted by Grimme’s D3 version with Becke-Johnson damping function.[5] Time-dependent DFT (TD-DFT) calculations were also carried out by this method. Vertical excitation calculations were based on optimized S0 geometries, and geometry optimizations for excited S1 and T1 states were carried out at the same level of theory. The analysis of hole and electron pair distributions was conducted using the Multiwfn code.[6,7]

## 1.7 Analysis of rate constants

The rate constants of radiative decay (kr,S) and nonradiative decay (knr,S) from S1 to S0 states, the rate constants of intersystem crossing (kISC) and reverse intersystem crossing (kRISC) were calculated from the following six equations:

kp=1/τp…………………………………………………………………Eq.(1)

kd=1/τd…………………………………………………………………Eq.(2)

kr,S= Φpkp+Φdkd≈Φpkp…………………………… ………………Eq.(3)

knr,S=1−ΦPLΦPLkr,S…………………………………………………………Eq.(4)

kISC=kp−kr,S−knr,S……………………………….…………………Eq.(5)

kRISC= kpkdΦd/kISCΦp……………………………………………Eq.(6)

Where τp and τd represent the prompt and decayed fluorescence lifetimes, respectively, which were determined from transient PL spectra. The kp and kd represent the decay rate constants for prompt and delayed fluorescence, respectively. Φp and Φd indicate prompt and delayed fluorescence components and can be distinguished from the total ΦPL by comparing the integrated intensities of prompt and delayed components in the transient PL spectra.

  - Device Fabrication and Measurement

Before OLED fabrication, DBFBN and DBFCN were purified by gradient sublimation using a BOF-A-5-60 apparatus (Anhui BEQ Equipment Technology Co., LTD) under a vacuum of 5 × 10⁻5 Pa. To evaluate the EL performance of DBFBN and DBFCN as emitter materials, we fabricated multilayered OLEDs. The ITO coated glass substrates with a sheet resistance of 15 Ω square-1 were ultrasonically cleaned with acetone/ethanol and dried with nitrogen gas flow, followed by 20 min ultraviolet light-ozone (UVO) treatment in a UV-ozone surface processor (PL16 series, Sen Lights Corporation). Organic layers were deposited at rates of 0.2-3 Å s-1 in a high vacuum chamber below 2.0 × 10-5 Pa in an inert gas glovebox. For all the devices, the emitting areas were determined by the overlap of two electrodes as 0.09 cm2. The as-fabricated devices were measured under ambient environment without any encapsulation. The current density-voltage-luminance (J-V-L), EQE-L curves and electroluminescence spectra were collected using a Keithley 2400 source meter and an absolute EQE measurement system (C9920-12, Hamamatsu Photonics, Japan). For operational lifetime measurements, the devices were encapsulated after fabrication, and the luminance decay was monitored under constant-current operation.

- Figures and Tables

Figure S1. Chemical structure and molecular design strategy of pure-green MR-TADF emitters.

Figure S2. 1H NMR spectrum of 1 in CDCl3.

Figure S3. 13C NMR spectrum of 1 in CDCl3.

Figure S4. 1H NMR spectrum of 2 in DMSO-d6.

Figure S5. 13C NMR spectrum of 2 in CDCl3.

Figure S6. 1H NMR spectrum of 3 in CDCl3.

Figure S7. 13C NMR spectrum of 3 in CDCl3.

Figure S8. 1H NMR spectrum of DBFCl in CDCl3.

Figure S9. 13C NMR spectrum of DBFCl in CDCl3.

Figure S10. 1H NMR spectrum of DBN in CD2Cl2.

Figure S11. 13C NMR spectrum of DBN in CDCl3.

Figure S12. 1H NMR spectrum of DBFBN in CDCl3.

Figure S13. 13C NMR spectrum of DBFBN in CDCl3.

Figure S14. HR-MS spectrum of DBFBN.

Figure S15. 1H NMR spectrum of DBFCN in CDCl3.

Figure S16. 13C NMR spectrum of DBFCN in CDCl3.

Figure S17. HR-MS spectrum of DBFCN.

Figure S18. Single-crystal structure of DBFCN (CCDC: 2542652).

Figure S19. The frontier molecular orbital distributions, energy levels, oscillator strengths, and excited-state energies of DBN-core (a), DBFBN-core (b), and DBFCN-core (c).

Figure S20. Natural transition orbital (NTO) distributions of S1 and T1 states for DBN-core, DBFBN-core, and DBFCN-core. The percentages denote the contribution weights of the displayed dominant NTO pair to the corresponding transition density.

Figure S21. Summary of reported green MR-TADF materials with FWHM ≤ 25 nm in dilute toluene.

Figure S22. Fluorescence spectra measured in solvents with different polarities (1.0×10-5 M) of DBN (a), DBFBN (b), and DBFCN (c).

Figure S23. The low temperature fluorescence and phosphorescence (measured at 77 K) spectra of DBN (a), DBFBN (b), and DBFCN (c) in toluene solution.

Figure S24. Transient photoluminescence decay curves of DBN (a), DBFBN (b), and DBFCN (c) in doped films.

Figure S25. The horizontal dipole ratio of DBFBN (a) and DBFCN (b) in doped films.

Figure S26. The Cyclic voltammetry curves of ferrocene (a), DBFBN (b), and DBFCN (c).

Figure S27. The TGA curve of DBFBN (a) and DBFCN (b).

Figure S28. (a) Device structures and energy level diagrams. (b) The molecular structures of relevant materials employed in devices.

Figure S29. Electroluminescent performance of the bottom-emitting green OLEDs containing DBFBN and DMIC-TRZ host at a concentration ratio of 3: 97. (a) Electroluminescence spectrum at 1000 cd m−2. (b) The EQE-L curve, (c) The PE-L and CE-L curve. (d) Current density and luminance versus voltage (J-V-L) characteristics.

Figure S30. CIE coordinates of the DBFBN- and DBFCN-based bottom-emitting OLEDs at 1000 cd m-2.

Figure S31. Absorption spectra of DBFCN as well as PL spectrum of Ir(ppy)3 in toluene solution (10-5 M).

Figure S32. Electroluminescent performance of the bottom-emitting green OLEDs containing DBFCN, Ir(ppy)3 sensitizer and DMIC-TRZ host at a concentration ratio of 2: 10: 88. (a) Device structures and energy level diagrams. (b) Electroluminescence spectrum at 1000 cd m-2. (c) CIE coordinates at 1000 cd m-2. (d) The EQE-L curve, PE-L, and CE-L curve. (e) Current density and luminance versus voltage (J-V-L) characteristics. (f) Operation lifetime of the sensitized devices at the initial luminance of 5000 cd m-2 (LT(1000 cd m-2) = LT(L₀) × [L₀ / (1000 cd m-2)]n, with an assumed acceleration factor of n = 1.75).[8]

Figure S33. Voltage-dependent EL spectra of the DBFCN-TE device.

Figure S34. Current density and luminance versus voltage (J-V-L) characteristics of the top-emitting green OLED.

Table S1. Crystal data and structure refinement for DBFCN.

| Identification code | DBFCN |
| --- | --- |
| Empirical formula | C76H54B2N6O2 |
| Formula weight | 1104.45 |
| Temperature/K | 170.00 |
| Crystal system | triclinic |
| Space group | P-1 |
| a/Å | 14.4827(7) |
| b/Å | 15.0673(7) |
| c/Å | 16.2981(8) |
| α/° | 99.087(2) |
| β/° | 111.687(2) |
| γ/° | 93.233(2) |
| Volume/Å3 | 3237.7(3) |
| Z | 2 |
| ρcalcg/cm3 | 1.308 |
| μ/mm-1 | 1.403 |
| F (000) | 1324.0 |
| Crystal size/mm3 | 0.16 × 0.08 × 0.06 |
| Radiation | Ga Kα (λ = 1.34139) |
| 2Θ range for data collection/° | 5.758 to 121.67 |
| Index ranges | -18 ≤ h ≤ 18, -19 ≤ k ≤ 19, -21 ≤ l ≤ 20 |
| Reflections collected | 49726 |
| Independent reflections | 14875 [Rint = 0.0801, Rsigma = 0.1492] |
| Data/restraints/parameters | 14875/0/783 |
| Goodness-of-fit on F2 | 1.072 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0718, wR2 = 0.2172 |
| Final R indexes [all data] | R1 = 0.1172, wR2 = 0.2360 |
| Largest diff. peak/hole / e Å-3 | 0.29/-0.26 |

Table S2. Summary of reported green MR-TADF materials with FWHM ≤ 25 nm in dilute toluene.

| Emitter | λPL [nm] | FWHMPL [nm] | Ref. |
| --- | --- | --- | --- |
| DBFBN | 507 | 14 | This work |
| DBFCN | 519 | 12 |  |
| BN-ICz-1 | 521 | 21 | Angew. Chem. Int. Ed. 2022, 61, e202202380. |
| BN-ICz-2 | 521 | 22 |  |
| v-DABNA-CN-Me | 496 | 17 | Adv. Mater. 2022, 34, 2201778. |
| DtCzBTPTRZ | 521 | 24 | CCS Chem. 2022, 4, 2065. |
| DBNO | 500 | 19 | Angew. Chem. Int. Ed. 2022, 61, e202200337 |
| tCzphB-Ph | 523 | 21 | Nat. Commun. 2022, 13, 4876. |
| tCzphB-Fl | 531 | 21 |  |
| ω-DABNA | 509 | 22 | J. Am. Chem. Soc. 2023, 145, 1505. |
| DBNT-2 | 512 | 20 | Nat. Photonics 2023, 17, 280. |
| 2PyBN | 499 | 21 | Chem. Sci.,2023, 14, 3326. |
| IDID2BN | 524 | 25 | Angew. Chem. Int. Ed. 2023, 62, e202313254. |
| DBF-DBN | 514 | 22 | Chem. Commun., 2023, 59, 5126. |
| DBT-DBN | 516 | 19 |  |
| BO-DICz | 507 | 18 | Angew. Chem. Int. Ed. 2023, e202318742. |
| TPABO-DICz | 515 | 17 |  |
| 6z | 516 | 22 | Angew. Chem. Int. Ed. 2024, 63, e202402020. |
| BNBO | 500 | 25 | Molecules 2024, 29, 841. |
| BpIC-DPA | 527 | 25 | Chem. Eng. J. 2024, 481, 148781. |
| ω-DABNA-M a | 514 | 23 | Nat. Commun. 2024 15, 3174. |
| SS-DAO | 512 | 21 | Angew. Chem. Int. Ed. 2024, 63, e202316710. |
| BpIC-DPA | 527 | 25 | Chem. Eng. J. 2024, 481, 148781. |
| BpIC-Cz | 534 | 22 |  |
| BN-2Pm | 505 | 20 | Chem. Eur. J. 2025, 31, e202404484. |
| ω’-DABNA | 513 | 19 | Angew. Chem. Int. Ed. 2025, 64, e202512162. |
| ω’-DABNA-D | 513 | 19 |  |
| QB-DPA | 495 | 15 | Angew. Chem. Int. Ed. 2025, 64, e202418348. |
| QB-PXZ | 508 | 15 |  |
| CNBN | 501 | 14 | Angew. Chem. Int. Ed. 2025,64, e202500108. |
| MCNBN | 510 | 15 |  |
| PCNBN | 503 | 18 |  |
| PMCNBN | 512 | 19 |  |
| DBNDS-TPh | 517 | 16 | Adv. Mater. 2025, 37, 2416224. |
| DBNDS-DFPh | 518 | 16.6 |  |
| DBNDS-CNPh | 518 | 16.4 |  |
| DBSe-BN | 514 | 21 | Adv. Mater. 2026,38, e13987. |
| DBNDO-1 | 512 | 14.8 | Angew. Chem. Int. Ed. 2025, e202515889. |
| DBNDO-2 | 517 | 14.1 |  |
| DBNDO-3 | 518 | 16.2 |  |
| tBN-NPTrz | 527 | 24 | Chem. Eng. J. 2025, 507, 160656. |
| tBN-DNPTrz | 529 | 22 |  |
| tBuICzBN-Ph | 522 | 22 | Chem. Eng. J. 2026, 530, 173453. |
| tBuICzBN-CN | 533 | 24 |  |
| tBuICzBN-Q | 536 | 23 |  |
| tBuICzBN-DPPM | 540 | 21 |  |
| HpCzB | 511 | 25 | Angew. Chem. Int. Ed. 2026, e23800. https://doi.org/10.1002/anie.202523800. |
| HpCzB-Fl | 531 | 22 |  |
| ω-DABNA-4TBP a | 519 | 23 | Adv. Sci. 2026, e22814. |
| ω-DABNA-4CzP a | 521 | 23 |  |
| ω-DABNA-4CNP a | 528 | 24 |  |
| DBF-v-DABNA | 517 | 16 | Adv. Mater. 2026, e18330. https://doi.org/10.1002/adma.202518330. |
| p-DBFSi | 517 | 15 | Adv. Mater. 2026, e72684. https://doi.org/10.1002/adma.72684 |
| m-DBFSi | 515 | 14 |  |
| m-DBFSi-d | 515 | 14 |  |

a Measured in a PMMA film

Table S3. Summary of fluorescence spectral data in solvents with different polarities.

| solvent | DBN |  | DBFBN |  | DBFCN |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | λPL [nm] | FWHMPL [nm] | λPL [nm] | FWHMPL [nm] | λPL [nm] | FWHMPL [nm] |
| n-hexane | 468 | 12 | 500 | 12 | 513 | 11 |
| Toluene | 475 | 14 | 507 | 14 | 519 | 12 |
| THF | 476 | 16 | 509 | 17 | 520 | 14 |
| DCM | 482 | 20 | 516 | 21 | 525 | 16 |

Table S4. Summary of rate constants in 3 wt% DMIC-TRZ-doped films.

| Emitter | kr,S [a] [107 s-1] | knr,S b [106 s-1] | kISC c [108 s-1] | kRISC d [105 s-1] |
| --- | --- | --- | --- | --- |
| DBN | 16.9 | 14.7 | 0.5 | 2.0 |
| DBFBN | 4.2 | 2.2 | 1.3 | 1.1 |
| DBFCN | 3.7 | 1.2 | 1.9 | 0.9 |

The rate constants of [a] radiative decay (kr,S), [b] non-radiative decay (knr,S), [c] intersystem crossing (kISC), [d] reverse intersystem crossing (kRISC).

Table S5. Summary of thermal and electrochemical data.

| Emitter | Td [oC] | HOMO [eV] | LUMO [eV] |
| --- | --- | --- | --- |
| DBFBN | 406 | −5.09 | −2.66 |
| DBFCN | 470 | −5.38 | −3.02 |

Table S6. Summary of reported performances of bottom-emitting OLEDs based on green MR-TADF emitters with CIEy ≥ 0.65. Note: binary-EML and ternary-EML OLEDs are shown in white and green background, respectively. No external light-extraction structures, such as microlens arrays or scattering films, were employed unless otherwise specified.

| Emitters | λEL [nm] | FWHM [nm] | CIE [x, y] | EQEmax [%] | CEmax [cd A−1] | PEmax [lm W−1] | Operational Lifetime | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| diboron skeleton |  |  |  |  |  |  |  |  |
| DBFCN | 521 | 13 | 0.18, 0.75 | 38.5 | 147.9 | 193.6 | - | This work |
|  | 521 | 14 | 0.21, 0.74 | 38.3 | 150.3 | 168.7 | LT50 = 618 h @5000 cd m−2 |  |
| DBTN-2 | 520 | 29 | 0.19, 0.74 | 35.2 | 132.9 | 130.4 | - | Nat. Photonics. 2023, 17, 280. |
| DBF-DBN | 521 | 31 | 0.22, 0.71 | 21.5 | - | 76.2 | - | Chem. Commun. 2023, 59, 5126. |
| DBT-DBN | 520 | 24 | 0.22, 0.70 | 31.3 | - | 93.6 | - |  |
| IDID2BN | 534 | 29 | 0.31, 0.65 | 36.6 | 146.3 | 135.2 | - | Angew. Chem. Int. Ed. 2023, 62, e202313254. |
| DBNDS-TPh | 524.6 | 19.3 | 0.17, 0.75 | 35.2 | 139.0 | - | LT50 < 1 h @5000 cd m-2 | Adv. Mater. 2025, 37, 2416224. |
|  | 524.6 | 19.6 | 0.20, 0.74 | 37.5 | 139.0 | - | LT50 ≈ 12 h @5000 cd m-2 |  |
| DBNDS-DFPh | 523.0 | 19.8 | 0.17, 0.76 | 34.5 | 136.0 | - | LT50 < 1 h @5000 cd m-2 |  |
|  | 523.0 | 20.3 | 0.19, 0.75 | 35.5 | 133.7 | - | LT50 ≈ 10 h @5000 cd m-2 |  |
| DBNDS-CNPh | 521.5 | 19.3 | 0.17, 0.75 | 29.8 | 113.0 | - | LT50 < 1 h @5000 cd m-2 |  |
|  | 523.0 | 20.5 | 0.19, 0.74 | 32.3 | 116.5 | - | LT50 ≈ 11 h @5000 cd m-2 |  |
| DBNDO-1 | 518.4 | 19 | 0.14, 0.75 | 31.1 | 113.9 | - | LT50 = 0.34 h @1000 cd m-2 | Angew. Chem. Int. Ed. 2025, e202515889. |
| DBNDO-2 | 520.7 | 19 | 0.16, 0.75 | 32.4 | 119.6 | - | LT50 = 0.43 h @1000 cd m-2 |  |
| DBNDO-3 | 524.4 | 19 | 0.18, 0.75 | 32.0 | 123.3 | - | LT50 = 0.53 h @1000 cd m-2 |  |
| CNBN | 506 | 16 | 0.12, 0.68 | 34.4 | 98.3 | 128.7 | - | Angew. Chem. Int. Ed. 2025, 64, e202500108. |
| MCNBN | 517 | 17 | 0.17, 0.74 | 30.8 | 111.4 | 145.8 | - |  |
| PCNBN | 508 | 20 | 0.14, 0.67 | 29.1 | 85.2 | 95.6 | - |  |
| PMCNBN | 519 | 22 | 0.19, 0.73 | 27.2 | 99.6 | 111.8 | - |  |
| W-DABNA | 534 | 33 | 0.28, 0.70 | 27.2 | 116.3 | 127.9 | LT90 = 16 h @1000 cd m-2 | Angew. Chem. Int. Ed. 2026, 65, e22105. |
|  | 533 | 34 | 0.27, 0.69 | 34.0 | - | - | LT80 = 19 h @5000 cd m-2 |  |
| W-DABNA-Cz | 515 | 27 | 0.15, 0.73 | 31.0 | 107.9 | 115.8 | LT90 = 20 h @1000 cd m-2 |  |
|  | 515 | 30 | 0.17, 0.72 | 36.1 | 124.8 | 117.5 | LT80 = 63 h @5000 cd m-2 |  |
| DBF-v-DABNA | 521 | 19 | 0.18, 0.75 | 25.8 | 100.2 | 130.0 | LT50 = 15 h @5000 cd m−2 | Adv. Mater. 2026, 38, e18330. |
|  | 521 | 20 | 0.21, 0.73 | 33.8 | 128.3 | 160.5 | LT50 = 645 h @5000 cd m−2 |  |
| p-DBFSi | 520 | 19 | 0.18, 0.74 | 37.2 | 140.7 | 165.4 | LT50 = 299 h @1000 cd m−2 | Adv. Mater. 2026, 38, e72684. |
|  | 521 | 20 | 0.19, 0.74 | 34.2 | 127.2 | 156.1 | LT80 = 85 h @5000 cd m−2 |  |
| m-DBFSi | 517 | 17 | 0.15, 0.76 | 40.1 | 143.2 | 187.5 | LT50 = 371 h @1000 cd m−2 |  |
|  | 518 | 18 | 0.18, 0.75 | 37.7 | 134.3 | 175.9 | LT80 = 120 h @5000 cd m−2 |  |
| m-DBFSi-d | 517 | 17 | 0.14, 0.76 | 41.9 | 146.7 | 191.8 | LT50 = 450 h @1000 cd m−2 |  |
|  | 518 | 18 | 0.17, 0.75 | 38.6 | 137.6 | 184.9 | LT80 = 149 h @5000 cd m−2 |  |
| multiboron skeleton (n ≥ 3, n is the number of B atoms) |  |  |  |  |  |  |  |  |
| ω-DABNA | 512 | 25 | 0.13, 0.73 | 31.1 | 101.0 | 98.1 | LT95 = 25 h @ 1000 cd m-2 LT80 = 292 h @ 1000 cd m-2 | J. Am. Chem. Soc. 2023, 145, 1505. |
| ω-DABNA-M | 515 | 25 | 0.15, 0.74 | 32.7 | - | 114.5 | LT95 = 24 h @ 1000 cd m-2 | Nat. Commun. 2024 15, 3174. |
|  | 517 | 23 | 0.17, 0.70 | 28.2 | - | 98.7 | LT95 = 110 h @ 1000 cd m-2 |  |
|  | 517 | 26 | 0.27, 0.66 | 19.1 | - | 67.3 | LT95 = 63 h @ 1000 cd m-2 |  |
| ω-DABNA-PH | 521 | 30 | 0.19, 0.74 | 31.8 | - | 27.4 | LT95 = 27 h @ 1000 cd m-2 |  |
|  | 522 | 29 | 0.21, 0.69 | 26.5 | - | 98.6 | LT95 = 109 h @ 1000 cd m-2 |  |
|  | 522 | 30 | 0.24, 0.70 | 24.4 | - | 107.5 | LT95 = 580 h @ 1000 cd m-2 |  |
| ω'-DABNA | 517 | 25 | 0.16, 0.73 | 32.3 | 118.0 | 154.5 | LT80 = 188 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2025, 64, e202512162. |
|  | 518 | 26 | 0.21, 0.77 | 33.4 | 122.2 | 143.9 | LT80 = 236 h @ 5000 cd m-2 |  |
| ω'-DABNA-D | 519 | 25 | 0.16, 0.75 | 34.6 | 128.5 | 155.5 | LT80 = 321 h @ 1000 cd m-2 |  |
|  | 519 | 26 | 0.20, 0.72 | 32.6 | 120.4 | 132.1 | LT80 = 394 h @ 5000 cd m-2 |  |
| QB-PXZ | 516 | 20 | 0.18, 0.74 | 36.6 | 134.8 | 151.3 | LT80 = 485 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2025, 64, e202418348. |
| ω-DABNA-4TBP | 526 | 25 | 0.20, 0.75 | 34.7 | 142.2 | 150.0 | LT95 = 28 h @ 1000 cd m-2 | Adv. Sci. 2026, e22814. |
|  | 523 | 25 | 0..19, 0.73 | 36.1 | 139.7 | 172.2 | LT95 = 384 h @ 1000 cd m-2 |  |
| ω-DABNA-4CzP | 528 | 25 | 0.22, 0.73 | 33.4 | 140.0 | 147.0 | LT95 = 2.2 h @ 1000 cd m-2 |  |
|  | 525 | 26 | 0.21, 0.71 | 35.1 | 135.0 | 155.3 | LT95 = 3.9 h @ 1000 cd m-2 |  |
| ω-DABNA-4CNP | 537 | 25 | 0.28, 0.70 | 32.8 | 145.8 | 153.8 | LT95 = 25 h @ 1000 cd m-2 |  |
|  | 533 | 26 | 0.25, 0.70 | 33.0 | 137.7 | 148.6 | LT95 = 1.4 h @ 1000 cd m-2 |  |
| monoboron skeleton |  |  |  |  |  |  |  |  |
| m-Cz-BNCz | 520 | 44 | 0.24, 0.69 | 27.4 | 102.2 | 107.1 | - | Angew. Chem. Int. Ed. 2020, 59, 17442. |
| AZA-BN | 527 | 30 | 0.27, 0.69 | 28.2 | - | 121.7 | LT90 = 46.3 h @ 2000 cd m-2 | Angew. Chem. Int. Ed. 2020, 59, 17499. |
| BBCz-G | 515 | 54 | 0.26, 0.68 | 31.8 | - | - | - | J. Am. Chem. Soc. 2020, 142, 19468. |
| PXZ-BN | 516 | 47 | 0.22, 0.67 | 23.3 | 83.8 | 70.1 | - | J. Mater. Chem. C 2021, 9, 8308. |
| TCz-B | 515 | 30 | 0.16, 0.71 | 29.2 | 100.7 | 72.4 | LT50 = 2.0 h @ 100 cd m-2 | Angew. Chem. Int. Ed. 2021, 60, 23142. |
| 2PTZBN | 528 | 58 | 0.28, 0.65 | 25.5 | 96.5 | 86.6 | - | Chem. Eng. J. 2021, 426, 131169. |
| v-DABNA-CN-Me | 504 | 23 | 0.13, 0.65 | 31.9 | 88.9 | 93.6 | - | Adv. Mater. 2022, 34, 2201778. |
| DBNO | 512 | 41 | 0.22, 0.67 | 33.1 | 114.4 | 115.9 | - | Angew. Chem. Int. Ed. 2022, 61, e202200337. |
| helicene-BN | 523 | 49 | 0.26, 0.66 | 31.5 | 117.5 | 153.8 | - | CCS Chem. 2022, 4, 3463. |
| BNSSe | 515 | 50 | 0.22, 0.66 | 35.7 | 124.2 | 156.2 | LT50 = 4.8 h @ 1000 cd m-2 | Nat. Photonics. 2022, 16, 803. |
| BNSeSe | 512 | 48 | 0.19, 0.66 | 36.8 | 121.0 | 146.3 | LT50 = 4.1 h @ 1000 cd m-2 |  |
| tCzphB-Ph | 527 | 24 | 0.21, 0.75 | 29.3 | - | - | - | Nat. Commun. 2022, 13, 4876. |
|  | 526 | 27 | 0.21, 0.74 | 31.3 | - | - | LT90 = 0.5 h @ 23300 cd m-2 |  |
| tCzphB-Fl | 535 | 26 | 0.26, 0.72 | 26.2 | - | - | - |  |
|  | - | - | 0.26, 0.71 | 29.7 | - | - | LT90 = 12.4 h @ 24500 cd m-2 |  |
| TCz-VTCzBN | 524 | 37 | 0.22, 0.71 | 32.2 | 96.7 | 129.3 | - | Angew. Chem. Int. Ed. 2022, 61, e202209984. |
| DtCzB-TPTRZ | 520 | 41 | 0.23, 0.68 | 30.6 | 105.8 | 116.2 | - | CCS Chem. 2022, 4, 2065. |
| BN-ICz-1 | 523 | 23 | 0.22, 0.74 | 20.5 | - | 84.2 | LT90 = 82.3 h @ 2000 cd m-2 | Angew. Chem. Int. Ed. 2022, 61, e202202380. |
| BN-ICz-2 | 52 | 23 | 0.23, 0.73 | 29.8 | - | 102.9 | LT90 = 71.3 h @ 2000 cd m-2 |  |
| TRZCzPh-BNCz | 513 | 37 | 0.17, 0.68 | 32.5 | - | 101.4 | LT50 = 13.4 h @ 500 cd m-2 | Angew. Chem. Int. Ed. 2022, 61, e202210210. |
| TRZTPh-BNCz | 513 | 33 | 0.16, 0.70 | 31.4 | - | 99.5 | LT50 = 14.7 h @ 500 cd m-2 |  |
| BN-TP | 528 | 36 | 0.26, 0.70 | 35.1 | 139.3 | 139.3 | LT50 = 28.8 h @ 4000 cd m-2 | Angew. Chem. Int. Ed. 2022, 61, e202204652. |
| BN-TP-N1 | 532 | 34 | 0.28, 0.69 | 34.9 | 137.7 | 139.7 | - | Angew. Chem. Int. Ed. 2023, 62, e202301930. |
|  | 532 | 34 | 0.30， 0.67 | 33.2 | 130.3 | 139.1 | - |  |
| BN-TP-N2 | 534 | 36 | 0.30, 0.67 | 31.9 | 129.5 | 139.8 | - |  |
|  | 534 | 35 | 0.30, 0.67 | 31.3 | 126.5 | 142.0 | - |  |
| BN-TP-N3 | 524 | 33 | 0.23, 0.71 | 37.3 | 135.5 | 139.9 | - |  |
|  | 524 | 34 | 0.26, 0.69 | 35.4 | 129.8 | 139.9 | - |  |
| BN-TP-N4 | 528 | 35 | 0.27, 0.70 | 36.5 | 136.3 | 143.2 | - |  |
|  | 528 | 36 | 0.28, 0.69 | 32.7 | 130.0 | 143.4 | - |  |
| BN-Py | 532 | 37 | 0.29, 0.68 | 30.6 | 119.6 | 118.9 | - | Adv. Mater. 2023, 35, 2305125. |
|  | 532 | 38 | 0.29, 0.68 | 31.0 | 110.6 | 110.1 | - |  |
| 2PyBN | 505 | 26 | 0.12, 0.65 | 37.1 | 106.7 | 139.6 | - | Chem. Sci., 2023, 14, 3326. |
| BN-STO | 517 | 34 | 0.19, 0.70 | 40.1 | 141.2 | 176.9 | LT50 = 35 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2023, 62, e202302478. |
| BN-XTO | 516 | 34 | 0.19, 0.70 | 37.3 | 131.0 | 156.9 | LT50 = 354 h @ 1000 cd m-2 |  |
| TPABO-DICz | 522 | 22 | 0.24, 0.74 | 25.8 | 84.1 | 100.5 | - | Angew. Chem. Int. Ed. 2043, 63, e202318742. |
| BNDCN | 507 | 30 | 0.13, 0.65 | 32.3 | 104.3 | 76.2 | - | Chem. Commun. 2024, 60, 574. |
| BNBO | 508 | 36 | 0.17, 0.65 | 24.3 | - | 62.2 | - | Molecules 2024, 29, 841. |
| h-BNCO-1 | 528 | 39 | 0.24, 0.71 | 40.1 | - | 147.0 | LT95 = 140 h @ 1000 cd m-2 | Nat. Commun. 2024, 15, 731. |
|  | 525 | 39 | 0.23, 0.71 | 25.1 | - | - | LT95 = 46 h @ 1000 cd m-2 | Nat. Commun. 2024, 15, 4394. |
|  | 529 | 39 | 0.26, 0.70 | 24.9 | - | - | LT95 = 124 h @ 1000 cd m-2 |  |
|  | 530 | 39 | 0.26, 0.68 | 16.3 | - | - | LT95 = 322 h @ 1000 cd m-2 |  |
|  | 530 | 39 | 0.27, 0.69 | 17.9 | - | - | LT95 = 437 h @ 1000 cd m-2 |  |
| tCzBN-PQ | 524 | 37 | 0.25, 0.67 | 30.2 | 115.6 | 94.3 | - | Chem. Eng. J. 2024, 481, 148794. |
| tCzBN-PQCz | 517 | 38 | 0.20, 0.69 | 35.1 | 131.0 | 106.9 | - |  |
| BThPAc-1 | 516 | 34 | 0.18, 0.72 | 24.8 | 87.9 | 98.7 | - | Chem. Sci. 2024, 15, 13290. |
| BThPAc-2 | 514 | 33 | 0.17, 0.72 | 25.8 | 89.9 | 106.8 | - |  |
| DCz-SFBN | 506 | 37 | 0.15, 0.65 | 29.2 | - | 89.7 | - | Mater. Horiz. 2024, 11, 4674. |
| DPhCz-SFBN | 522 | 37 | 0.22, 0.70 | 31.0 | - | 122.2 | - |  |
|  | 520 | 37 | 0.23, 0.69 | 31.1 | - | 140.9 | - |  |
| CzTCz-SFBN | 518 | 35 | 0.20, 0.71 | 28.1 | - | 103.0 | - |  |
|  | 521 | 37 | 0.22, 0.68 | 26.2 | - | 110.7 | - |  |
| 3CzSF-BN | 522 | 36 | 0.21, 0.72 | 20.3 | 76.2 | 88.7 | - | Adv. Optical Mater. 2024, 12, 2400490. |
|  | 519 | 37 | 0.20, 0.71 | 23.1 | 82.9 | 66.8 | - |  |
| Th-BN | 516 | 41 | 0.23, 0.68 | 34.6 | 122.9 | 134.3 | - | Chem. Sci. 2024, 15, 11435. |
| SBNO | 524 | 40 | 0.26, 0.68 | 25.7 | 86.4 | 71.4 | - | Small 2024, 20, 2407220. |
| SBNOS | 522 | 40 | 0.25, 0.69 | 32.7 | 99.7 | 80.3 | - |  |
| BpIC-DPA | 536 | 29 | 0.30, 0.67 | 22.0 | 94.0 | 98.8 | LT90 = 156.1 h @ 1000 cd m-2 | Chem. Eng. J. 2024, 481, 148781. |
| m-ICz-BNCz | 516 | 40 | 0.20, 0.70 | 28.0 | - | 81.9 | - | Adv. Optical Mater. 2024, 12, 2400200. |
| dm-ICz-BNCz | 534 | 46 | 0.30, 0.67 | 32.9 | - | 105.8 | - |  |
| Spiro-BNCz | 533 | 48 | 0.29, 0.67 | 34.2 | 140.5 | 90.1 | - | Aggregate. 2024, 5, e445. |
| TCzBAO | 520 | 36 | 0.20, 0.70 | 25.1 | 90.5 | 101.5 | - | Adv. Optical Mater. 2024, 12, 2301711. |
| 6z | 513 | 27 | 0.18, 0.70 | 31.7 | 109.2 | 122.6 | - | Angew. Chem. Int. Ed. 2024, 63, e202402020. |
|  | 515 | 36 | 0.28, 0.65 | 27.0 | 92.5 | 73.6 | - |  |
| 2SBN | 514 | 45 | 0.20, 0.65 | 27.1 | 74.90 | 71.48 | - | Adv. Optical Mater. 2024, 12, 2401754. |
| 3SBN | 514 | 43 | 0.20, 0.66 | 27.0 | 90.3 | 55.6 | - |  |
| MesPXZ-tCzBN | 528 | 54 | 0.31, 0.65 | 27.6 | 110.6 | 150.3 | - | Adv. Optical Mater. 2024, 13, 2402131. |
| BN-2Pm | 514 | 27 | 0.17, 0.71 | 32.8 | 92.3 | 76.3 | - | Chem. Eur. J. 2025, 31, e202404484. |
| DBSe-BN | 517 | 24 | 0.18, 0.73 | 38.8 | 139.3 | 156.3 | LT50 = 1341 h @ 1000 cd m-2 | Adv. Mater. 2026, 38, e13987. |
|  | 518 | 25 | 0.22, 0.71 | 33.4 | 123.4 | 136.1 | LT50 = 318 h @ 5000 cd m-2 |  |
| m-PAz-BNCz | 528 | 37 | 0.26, 0.70 | 36.2 | 132.1 | 133.9 | - | Adv. Mater. 2025, 37, 2503383. |
|  | 528 | 39 | 0.28, 0.68 | 35.7 | 135.3 | 152.1 | - |  |
| m-SFAz-BNCz | 532 | 38 | 0.28, 0.69 | 33.7 | 129.1 | 128.1 | - |  |
|  | 532 | 40 | 0.30, 0.67 | 31.2 | 123.8 | 143.1 | - |  |
| m-DPAcPAz-BNCz | 524 | 37 | 0.24, 0.70 | 33.8 | 129.0 | 135.1 | - |  |
|  | 524 | 40 | 0.27, 0.68 | 33.8 | 124.2 | 143.6 | - |  |
| m-TPAz-BNCz | 532 | 38 | 0.28, 0.69 | 33.9 | 125.2 | 131.1 | - |  |
|  | 532 | 40 | 0.29, 0.67 | 32.2 | 121.7 | 139.9 | - |  |
| tBN-DNPTrz | 532 | 36 | 0.29, 0.67 | 29.3 | 103.8 | - | LT95 = 360 h @ 5000 cd m-2 | Chem. Eng. J. 2025, 507, 160656. |
| ACz-BN1 | 520 | 41 | 0.218, 0.685 | 34.8 | 123.7 | 155.4 | - | Adv. Optical Mater. 2025, 13, 2501147. |
| ACz-BN2 | 524 | 41 | 0.218, 0.685 | 27.2 | 98.8 | 124.1 | - |  |
| ACz-BN3 | 527 | 41 | 0.239, 0.692 | 26.6 | 98.3 | 118.7 | - |  |
| ACz-BN4 | 530 | 43 | 0.254, 0.679 | 42.4 | 122.5 | 147.9 | - |  |
| AZP-BN | 510 | 30 | 0.134, 0.687 | 34.2 | 107.7 | 116.6 | - | Sci. China Chem. 2026, 69, 2958. |
| APT-BN1 | 514 | 32 | 0.156, 0.701 | 30.1 | 101.1 | 116.0 | - |  |
| APT-BN2 | 512 | 32 | 0.153, 0.699 | 31.2 | 112.0- | 112.0 | - |  |
| APT-Ph-BN | 520 | 32 | 0.187, 0.715 | 39.6 | 126.2 | 140.5 | - |  |
| tBuICzBN-Ph | 524 | 28 | 0.23, 0.69 | 21.8 | 73.7 |  | LT97 = 3.8 h @ 5000 cd m-2 | Chem. Eng. J. 2026, 530, 173453. |
| tBuICzBN-Ph | 525 | 28 | 0.24, 0.71 | 28.7 | 96.7 |  | LT97 = 118 h @ 5000 cd m-2 |  |
| tBuICzBN-CN | 535 | 36 | 0.31, 0.66 | 25.8 | 91.0 |  | LT97 = 55.0 h @ 5000 cd m-2 |  |
| tBuICzBN-Q | 540 | 28 | 0.31, 0.35 | 19.4 | 70.9 |  | LT97 = 5.8 h @ 5000 cd m-2 |  |
| tBuICzBN-Q | 540 | 30 | 0.32, 0.66 | 28.9 | 104.6 |  | LT97 = 143 h @ 5000 cd m-2 |  |
| tBuICzBN-DPPM | 541 | 33 | 0.32, 0.65 | 26.5 | 92.2 |  | LT97 = 157 h @ 5000 cd m-2 |  |
| DBCzB-Fl | 534 | 33 | 0.31, 0.66 | 20.5 | 83.9 | 94.1 | LT90 = 264 h @ 5000 cd m-2 | Angew. Chem. Int. Ed. 2026, 65, e23800. |
| HpCzB-Fl | 534 | 29 | 0.32, 0.67 | 27.7 | 113.0 | 126.8 | LT90 = 616 h @ 5000 cd m-2 |  |
| BCzBNSS-2 | 519 | 27 | 0.20, 0.72 | 26.2 | 87.7 | 84.6 | - | Angew. Chem. Int. Ed. 2026, 65,e23890. |
| BCzBNSSe | 520 | 27 | 0.20, 0.72 | 31.3 | 103.3 | 92.0 | - |  |

Table S7. Summary of reported performances of top-emitting OLEDs based on pure-green MR-TADF emitters. No external light-extraction structures, such as microlens arrays or scattering films, were employed unless otherwise specified.

| Emitters | λEL [nm] | FWHM [nm] | CIE [x, y] | EQEmax [%] | CEmax [cd A−1] | PEmax [lm W−1] | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DBFCN | 522 | 13 | 0.14, 0.79 | 58.9 | 232.5 | 304.2 | This work |
| BN-ICz-1 | 525 | 19 | 0.17, 0.78 | - | 220 | - | Angew. Chem. Int. Ed. 2022, 61, e202202380. |
| TPABO-DICz | 524 | 16 | 0.14, 0.79 | 55.2 | 226.4 | 278.3 | Angew. Chem. Int. Ed. 2024, 63, e202318742. |
| ACz-BN1 | 523 | 19.9 | 0.142, 0.782 | 47.6 | 184.4 | 231.7 | Adv. Optical Mater. 2025, 13, 2501147. |
| ACz-BN2 | 524 | 20.5 | 0.146, 0.780 | 44.8 | 175.3 | 203.9 |  |
| ACz-BN3 | 527 | 20.1 | 0.164, 0.778 | 52.2 | 213.7 | 256.4 |  |
| ACz-BN4 | 530 | 21.3 | 0.190, 0.765 | 47.1 | 200.4 | 233.1 |  |
| tBN-DNPTrz | 530 | 20 | 0.19, 0.76 | - | 195.3 | - | Chem. Eng. J. 2025, 507, 160656. |
| AZP-BN | 512 | 17.0 | 0.063, 0.749 | 55.8 | 166.8 | 199.8 | Sci. China Chem. 2026, 69, 2958. |
| APT-BN1 | 513 | 16.9 | 0.068, 0.757 | 56.6 | 174.1 | 203.9 |  |
| APT-BN2 | 514 | 17.4 | 0.074, 0.764 | 57.9 | 182.9 | 217.4 |  |
| APT-Ph-BN | 524 | 17.8 | 0.144, 0.789 | 54.2 | 215.6 | 250.8 |  |
| DBF-v-DABNA | 521 | 16 | 0.14, 0.79 | - | 233 | - | Adv. Mater. 2026, 38, e18330. |

Table S8. Comparative summary of EL spectral evolution from bottom-emitting to top-emitting OLEDs based on green MR-TADF emitters. No external light-extraction structures, such as microlens arrays or scattering films, were employed unless otherwise specified.

| Emitters | Bottom-emitting OLEDs |  |  | Top-emitting OLEDs |  |  | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | λEL [nm] | FWHM [nm] | CIE [x, y] | λEL [nm] | FWHM [nm] | CIE [x, y] |  |
| DBFCN | 521 | 14 | 0.21,0.74 | 522 | 13 | 0.14,0.79 | This work |
| BN-ICz-1 | 523 | 23 | 0.22, 0.74 | 525 | 19 | 0.17, 0.78 | Angew. Chem. Int. Ed. 2022, 61, e202202380. |
| TPABO-DICz | 522 | 22 | 0.24, 0.74 | 524 | 16 | 0.14, 0.79 | Angew. Chem. Int. Ed. 2024, 63, e202318742. |
| ACz-BN1 | 520 | 41 | 0.218, 0.685 | 523 | 19.9 | 0.142, 0.782 | Adv. Optical Mater. 2025, 13, 2501147. |
| ACz-BN2 | 524 | 41 | 0.218, 0.685 | 524 | 20.5 | 0.146, 0.780 |  |
| ACz-BN3 | 527 | 41 | 0.239, 0.692 | 527 | 20.1 | 0.164, 0.778 |  |
| ACz-BN4 | 530 | 43 | 0.254, 0.679 | 530 | 21.3 | 0.190, 0.765 |  |
| tBN-DNPTrz | 531 | 35 | 0.9, 0.67 | 530 | 20 | 0.19, 0.76 | Chem. Eng. J. 2025, 507, 160656. |
| AZP-BN | 510 | 30 | 0.134, 0.687 | 512 | 17.0 | 0.063, 0.749 | Sci. China Chem. 2026, 69, 2958. |
| APT-BN1 | 514 | 32 | 0.156, 0.701 | 513 | 16.9 | 0.068, 0.757 |  |
| APT-BN2 | 512 | 32 | 0.153, 0.699 | 514 | 17.4 | 0.074, 0.764 |  |
| APT-Ph-BN | 520 | 32 | 0.187, 0.715 | 524 | 17.8 | 0.144, 0.789 |  |
| DBF-v-DABNA | 521 | 20 | 0.21, 0.73 | 521 | 16 | 0.14, 0.79 | Adv. Mater. 2026, 38, e18330. |

- References

- M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria, M. A. Robb, J. R. Cheeseman, G. Scalmani, V. Barone, G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. Marenich, J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian, J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, D. Williams-Young, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. A. Montgomery, Jr., J. E. Peralta, F. Ogliaro, M. Bearpark, J. J. Heyd, E. Brothers, K. N. Kudin, V. N. Staroverov, T. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi, J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, and D. J. Fox, Gaussian, Inc., Wallingford CT, 2016.

- A. D. Becke, J. Chem. Phys. 1993, 98, 5648.

- P. C. Hariharan, J. A. Pople, Theoret. Chim. Acta, 1973, 28, 213.

- R. Ditchfield, W. J. Hehre, J. A. Pople, J. Chem. Phys. 1971, 54, 724.

- L. Goerigk, A. Hansen, C. Bauer, S. Ehrlich, A. Najibi, S. Grimme, Phys. Chem. Chem. Phys. 2017, 19, 32184.

- T. Lu, F. Chen, J. Comput. Chem. 2012, 33, 580.

- Z. Liu, T. Lu, Q. Chen, Carbon 2020, 165, 461.

- X. Cai, Y. Xu, Y. Pan, L. Li, Y. Pu, X. Zhuang, C. Li, Y. Wang, Angew. Chem. Int. Ed. 2023, 62, e202216473.