Supporting Information

Tetraphenylsilane-Engineered MR-TADF Emitters for Pure-Green OLEDs with High-Efficiency, Long Lifetime and Gamut Close to BT.2020 Standard

Zhuixing Xue, Yuxuan Hu*, Zhiyi Chen, Xiudan Zhang, Jingsheng Miao, and Chuluo Yang*

Shenzhen Key Laboratory of New Information Display and Storage Materials, College of Materials Science and Engineering, Shenzhen University, Shenzhen, 518060 (P. R. China)

Corresponding Authors

Yuxuan Hu, Email: huyuxuan@szu.edu.cn

Chuluo Yang, Email: clyang@szu.edu.cn

Table of Contents

- Experimental sectionS3

1.1 Materials and MethodsS3

1.2 SynthesisS3

1.3 Single Crystal X-ray CrystallographyS7

1.4 Thermal and Electrochemical characterizationS7

1.5 Photophysical characterizationS8

1.6 Quantum chemical calculationsS8

1.7 Analysis of rate constantsS8

1.8 Device Fabrication and MeasurementS9

2. Figures and TablesS10

3. ReferencesS49

- Experimental section

## 1.1 Materials and Methods

All reagents were used as received from commercial sources without further purification unless otherwise mentioned. Solvents for chemical synthesis were purified according to the standard procedures. All reactions were heated by metal sand bath (WATTCAS, LAB-500, https://www.wattcas.com). NMR spectra were measured on Bruker Advance spectrometers (400 MHz and 500 MHz for 1H NMR, and 101/126 MHz for 13C NMR). Tetramethylsilane was used as the internal standard and CDCl3 as the solvent. The high-resolution mass spectrometry (HR-MS) for the compounds was conducted on a Thermo Scientific LTQ Orbitrap XL with ESI ion source.

## 1.2 Synthesis

Scheme S1. Synthetic route of p-DBFSi, m-DBFSi and m-DBFSi-d.

Synthesis of 1: Under argon atmosphere, a mixture of compound 2-bromodibenzo[b,d]furan (6.0 g, 24.28 mmol), 2,6-dimethylaniline (3.53 g, 29.14 mmol), Pd2(dba)3 (200 mg, 0.24 mmol), S-Phos (598 mg, 1.46 mmol) and tBuONa (4.20 g, 43.71 mmol) in 50 mL deoxygenated solution (xylenes) was stirred at 120 °C for 6 h. After cooling to room temperature, the crude product was precipitated by adding water, and then filtered and repeatedly washed with ethanol three to four times to afford the product as a white solid 1 (6.4 g, yield: 92%). 1H NMR (500 MHz, CDCl3) δ (ppm): 7.78 (d, J = 7.7 Hz, 1H), 7.49 (d, J = 8.1 Hz, 1H), 7.43 – 7.33 (m, 2H), 7.24 (t, J = 7.5 Hz, 1H), 7.16 (d, J = 7.3 Hz, 2H), 7.13 – 7.07 (m, 1H), 6.95 (d, J = 2.4 Hz, 1H), 6.74 (dd, J = 8.8, 2.5 Hz, 1H), 5.25 (s, 1H), 2.24 (s, 6H). 13C NMR (126 MHz, CDCl3) δ (ppm): 156.88, 150.39, 142.45, 139.11, 135.54, 128.86, 126.95, 125.62, 124.98, 124.55, 122.27, 120.74, 114.99, 112.09, 111.68, 104.34, 18.51.

Synthesis of 2: Under argon atmosphere, intermediate 1 (4.0 g, 13.91 mmol), 1,3-dibromo-5-chlorobenzene (11.29 g, 41.75 mmol), Pd2(dba)3 (128 mg, 0.14 mmol), S-Phos (285 mg, 0.70 mmol) and tBuONa (4.12 g, 27.82 mmol) were added into a 200 mL two-neck flask. Then, 40 mL deoxygenated solution (xylenes) was injected into the mixture. The reaction was refluxed for 6 h at 100 ºC. After cooling to room temperature, the reaction mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 4:1, ν/ν), giving the intermediate 2 as a white solid (5.31 g, yield 80%). 1H NMR (500 MHz, CDCl3) δ (ppm): 7.84 (dd, J = 7.7, 1.3 Hz, 1H), 7.58 – 7.52 (m, 2H), 7.48 – 7.42 (m, 2H), 7.30 (td, J = 7.5, 1.0 Hz, 1H), 7.23 – 7.14 (m, 4H), 6.97 (t, J = 1.7 Hz, 1H), 6.89 (t, J = 1.9 Hz, 1H), 6.76 (t, J = 2.0 Hz, 1H), 2.10 (s, 6H). 13C NMR (126 MHz, CDCl3) δ (ppm): 156.95, 152.46, 149.53, 141.99, 139.91, 137.57, 135.88, 129.79, 127.93, 127.53, 125.23, 124.02, 123.48, 122.73, 122.44, 122.42, 120.94, 118.44, 116.09, 114.31, 112.39, 111.85, 18.98.

Synthesis of 3: Under argon atmosphere, intermediate 2 (3.5 g, 7.34 mmol), N1,N3-bis(2,6-dimethylphenyl)benzene-1,3-diamine (1.01g, 3.19 mmol), Pd2(dba)3 (116 mg, 0.13 mmol), S-Phos (105 mg, 0.25 mmol) and tBuONa (1.22 g, 12.76 mmol) were added into a 200 mL two-neck flask. Subsequently, 40 mL deoxygenated solution (xylenes) was injected into the mixture, which was refluxed for 8 h at 120ºC. After cooling to room temperature, the mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed under reduced pressure, then the crude product was purified by silica gel column chromatography (eluent: petroleum ether/dichloromethane = 4:1, ν/ν), giving the intermediate 3 as a white solid (2.76 g, yield 78%). 1H NMR (500 MHz, CDCl3) δ (ppm): 7.79 (d, J = 1.3 Hz, 2H), 7.53 (d, J = 8.2 Hz, 2H), 7.45 – 7.40 (m, 4H), 7.32 – 7.26 (m, 4H), 7.13 – 7.10 (m, 1H), 7.09 (s, 1H), 7.05 (d, J = 7.5 Hz, 4H), 7.01 (d, J = 2.5 Hz, 1H), 6.99 (d, J = 2.4 Hz, 1H), 6.94 (dd, J = 8.3, 6.6 Hz, 2H), 6.87 (d, J = 7.5 Hz, 4H), 6.81 (t, J = 8.1 Hz, 1H), 6.50 (dd, J = 8.2, 2.2 Hz, 2H), 6.39 (t, J = 2.1 Hz, 2H), 6.33 (t, J = 1.9 Hz, 2H), 6.24 (t, J = 2.0 Hz, 2H), 6.16 (t, J = 2.2 Hz, 1H), 1.99 (s, 12H), 1.86 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 156.84, 151.69, 148.54, 147.35, 145.84, 142.44, 141.85, 140.85, 137.63, 137.31, 135.45, 129.38, 129.17, 129.01, 127.32, 127.22, 124.79, 124.18, 122.49, 121.27, 120.77, 112.87, 112.69, 112.01, 111.85, 111.75, 111.21, 110.83, 107.64, 18.72, 18.24.

Synthesis of DBFCl: In a 200 mL sealed tube charged with argon, a solution of intermediate 3 (2.0 g, 1.80 mmol) in 20 ml of highly dry 1,2-dichlorobenzene was prepared. After boron tribromide (12.0 equiv.) was added, the tube was sealed and then the reaction was heated and stirred at 200ºC for 48 h. Upon cooling to ambient temperature, the reaction was quenched by the dropwise addition of ethanol (10.0 mL) under an ice bath. The accumulated organic solvent was concentrated in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 3:1, ν/ν), yielding the intermediate DBFCl (1.46 g, 72% yield) as yellow solids. 1H NMR (500 MHz, CDCl3) δ (ppm): 10.86 (s, 1H), 9.56 (s, 2H), 7.89 (d, J = 7.7 Hz, 2H), 7.55 (t, J = 8.8 Hz, 3H), 7.52 – 7.48 (m, 3H), 7.45 (d, J = 7.5 Hz, 4H), 7.31 (t, J = 7.4 Hz, 2H), 7.26 – 7.20 (m, 4H), 7.11 (d, J = 7.7 Hz, 4H), 6.29 (d, J = 1.6 Hz, 2H), 6.25 (d, J = 1.6 Hz, 2H), 5.74 (s, 1H), 2.00 (s, 12H), 1.85 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 156.96, 151.10, 147.57, 145.23, 145.20, 142.72, 141.01, 138.34, 137.34, 136.69, 135.83, 129.03, 128.40, 128.04, 127.66, 127.36, 127.31, 123.78, 123.35, 121.17, 120.50, 118.25, 115.14, 113.84, 110.76, 106.04, 105.50, 105.32, 98.68, 16.64, 16.34.

Synthesis of p-DBFSi, m-DBFSi and m-DBFSi-d: Under argon atmosphere, intermediate DBFCl (300 mg, 0.27 mmol), (4-(triphenylsilyl)phenyl)boronic acid (308 mg, 0.81 mmol)/triphenyl(3-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)phenyl)silane (375 mg, 0.81 mmol)/tris(phenyl-d5)(3-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)phenyl-2,4,5,6-d4)silane (390 mg, 0.81 mmol), Pd(PPh3)4 (34 mg, 0.03 mmol) and K2CO3 (149 mg, 1.08 mmol) were added into a 100 mL two-neck flask. Then, 25 mL deoxygenation solution (Toluene: Ethanol: H2O = 2:1:1) was injected into the mixture. The reaction was refluxed for 8 h at 80 ºC. After cooling to room temperature, the reaction mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed in vacuum, and then the resultant crude product underwent purification through the employment of silica gel column chromatography (eluent: petroleum ether/dichloromethane = 2:1, ν/ν), giving p-DBFSi (405 mg, yield 87%), m-DBFSi (390 mg, yield 82%) and m-DBFSi-d (366 mg, yield 82%) as orange solid

p-DBFSi: 1H NMR (500 MHz, CDCl3) δ (ppm): 10.91 (s, 1H), 9.63 (s, 2H), 7.89 (d, J = 6.4 Hz, 2H), 7.57 (d, J = 8.2 Hz, 2H), 7.56 – 7.53 (m, 12H), 7.52 (dd, J = 7.1, 1.2 Hz, 2H), 7.47 (m, 7H), 7.45 – 7.40 (m, 10H), 7.36 (m, 13H), 7.33 – 7.29 (m, 6H), 7.28 (s, 2H), 7.21 (t, J = 7.7 Hz, 2H), 7.09 (d, J = 7.7 Hz, 4H), 6.43 (s, 2H), 6.41 (s, 2H), 5.78 (s, 1H), 2.04 (s, 12H), 1.89 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 158.02, 152.01, 149.01, 145.85, 145.24, 143.74, 142.98, 142.56, 139.95, 138.98, 138.01, 137.11, 136.69, 136.43, 134.17, 133.32, 129.93, 129.65, 129.31, 128.88, 128.46, 128.15, 127.93, 126.89, 125.13, 124.61, 122.11, 121.51, 119.24, 116.30, 115.95, 111.81, 106.07, 102.85, 102.41, 99.30, 17.81, 17.52. HR-MS (ESI) m/z [M+H]+ calcd for C122H92B2N4O2Si2+ 1723.7018, found 1723.6972.

m-DBFSi: 1H NMR (500 MHz, CDCl3) δ (ppm): 10.88 (s, 1H), 9.61 (s, 2H), 7.88 (d, J = 7.6 Hz, 2H), 7.56 (d, J = 8.1 Hz, 2H), 7.50 (d, J = 6.5 Hz, 18H), 7.48 – 7.42 (m, 8H), 7.41 – 7.27 (m, 26H), 7.15 (t, J = 7.7 Hz, 2H), 7.03 (d, J = 7.6 Hz, 4H), 6.27 (s, 2H), 6.26 (s, 2H), 5.73 (s, 1H), 1.97 (s, 12H), 1.83 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 157.98, 151.95, 148.95, 146.07, 145.73, 143.65, 142.53, 141.89, 139.84, 138.86, 137.89, 136.98, 136.38, 135.43, 134.69, 134.07, 129.80, 129.56, 129.20, 129.08, 128.71, 128.32, 128.11, 128.04, 127.98, 127.92, 125.10, 124.60, 122.06, 121.47, 119.15, 116.27, 115.62, 111.79, 106.03, 103.23, 102.74, 99.27, 17.75, 17.45. HR-MS (ESI) m/z [M+H]+ calcd for C122H54D38B2N4O2Si2+ 1723.7018, found 1723.6990.

m-DBFSi-d: 1H NMR (500 MHz, CDCl3) δ (ppm): 10.88 (s, 1H), 9.61 (s, 2H), 7.88 (d, J = 7.6 Hz, 2H), 7.56 (d, J = 8.1 Hz, 2H), 7.50 (t, J = 7.7 Hz, 2H), 7.41 – 7.36 (m, 2H), 7.34 (d, J = 6.5 Hz, 4H), 7.30 (t, J = 7.4 Hz, 2H), 7.25 (d, J = 1.8 Hz, 2H), 7.15 (t, J = 7.6 Hz, 2H), 7.03 (d, J = 7.7 Hz, 4H), 6.27 (s, 2H), 6.26 (s, 2H), 5.73 (s, 1H), 1.97 (s, 12H), 1.83 (s, 12H). 13C NMR (126 MHz, CDCl3) δ (ppm): 158.01, 151.98, 148.98, 146.05, 145.76, 142.56, 141.75, 139.87, 138.88, 137.91, 137.00, 136.12, 135.94, 135.75, 135.02, 134.52, 133.86, 129.83, 129.23, 129.06, 128.74, 128.34, 128.14, 128.08, 127.61, 127.42, 127.23, 125.12, 124.62, 122.09, 121.49, 119.18, 116.29, 115.65, 111.81, 106.06, 103.25, 102.76, 99.30, 17.77, 17.48. HR-MS (ESI) m/z [M+H]+ calcd for C122H92B2N4O2Si2+ 1761.9403, found 1761.9359.

Scheme S2. Synthetic route of DBFBN.

Synthesis of DBFBN: Under argon atmosphere, intermediate DBFCl (350 mg, 0.31 mmol), Pd2(dba)3 (14 mg, 0.02 mmol), S-Phos (13 mg, 0.03 mmol) and tBuOK (209 mg, 1.87 mmol) were added into a 100 mL two-neck flask. Subsequently, deoxygenated EtOH (86 mg, 1.87 mmol) and 15 mL deoxygenated solution (xylenes) were injected into the mixture, which was refluxed for 1 h at 120 ºC. After cooling to room temperature, the mixture was extracted three times with dichloromethane and water, and the accumulated organic layer was condensed under reduced pressure, then t the crude product was purified by silica gel column chromatography (eluent: petroleum ether/dichloromethane = 5:2, ν/ν), giving the intermediate DBFBN as a yellow solid (233 mg, yield 71%). 1H NMR (500 MHz, CDCl3) δ (ppm): 10.90 (s, 1H), 9.61 (s, 2H), 7.89 (d, J = 7.6 Hz, 2H), 7.56 (d, J = 8.1 Hz, 2H), 7.51 (d, J = 7.4 Hz, 2H), 7.49 – 7.45 (m, 2H), 7.43 (d, J = 7.4 Hz, 4H), 7.32 – 7.27 (m, 6H), 7.21 (t, J = 7.7 Hz, 2H), 7.09 (d, J = 7.7 Hz, 4H), 6.12 (t, J = 8.7 Hz, 4H), 5.77 (s, 1H), 2.01 (s, 12H), 1.86 (s, 12H). 13C NMR (101 MHz, CDCl3) δ (ppm): 157.98, 151.92, 148.75, 145.36, 143.84, 142.31, 140.09, 139.12, 138.07, 137.16, 133.16, 129.82, 129.16, 128.66, 128.25, 128.12, 124.59, 122.06, 121.47, 116.30, 111.78, 105.96, 104.08, 103.49, 99.07, 17.72, 17.42.

## 1.3 Single Crystal X-ray Crystallography

X-ray single crystal data was collected on a Bruker D8 Venture diffractometer using CuKα radiation (λ = 1.54178) source. The selected crystal was kept at 170.0 K during data collection. Using Olex21, the structure was solved with the ShelXT2 structure solution program using Intrinsic Phasing and refined with the ShelXL3 refinement package using Least Squares minimization. Selected crystal data are listed in Table S1-S2. All crystallographic information in CIF format have been deposited at the Cambridge Crystallographic Data Center (CCDC) under deposition number of 2504406 for p-DBFSi and 2504404 for m-DBFSi via www.ccdc.cam.ac.uk/data_request/cif, or by emailing data_request@ccdc.cam.ac.uk, or by contacting the Cambridge Crystallographic Data Center, 12 Union Road, Cambridge CB2 1EZ, UK; fax: +44 1223 336033.

## 1.4 Thermal and Electrochemical characterization

Thermogravimetric analysis (TGA) was undertaken using TGA-Q50 Instrument (TA Instruments, America) at a heating rate of 10 °C/min from 50°C to 700°C under nitrogen flushing. The thermal decomposition temperatures (Td) were determined by the recorded temperature at 5% weight loss. Cyclic voltammetry (CV) measurements were performed on a CH1660E electrochemical workstation using n-Bu4NPF6 (0.1 M) in dichloromethane (DCM) as electrolyte solution and ferrocene as an internal reference at a scan rate of 0.1 V s–1. The CV cell consisted of a glassy carbon electrode, a Pt wire counter electrode, and a standard Ag/AgCl reference electrode. The polymers were spin-coated on the working electrode for measurements. The redox potentials were calibrated with ferrocene as an internal standard. The highest occupied molecular orbital (HOMO) energy levels of the polymers were estimated by the equation: EHOMO = ‒ (4.80 + Eonsetox) eV. The lowest unoccupied molecular orbital (LUMO) energy levels of the polymers were calculated by ELUMO = EHOMO + Eg, and Eg is the optical band gap calculated from the absorption onset in dilute toluene (10-5 M).

## 1.5 Photophysical characterization

The UV-vis absorption spectra were obtained on a Shimadzu UV-2600 spectrophotometer (Shimadzu, Japan) at room temperature with a concentration of 1×10-5 M. Phosphorescence spectra were measured on a Hitachi F-7100 fluorescence spectrophotometer at 77 K. The transient photoluminescence (PL) decay curves were obtained by FluoTime 300 (PicoQuant GmbH) with a Picosecond Pulsed UV-LASTER (LASTER375) as the excitation source. The solid-state PL quantum efficiencies (ΦPLs) were measured on a Hamamatsu UV-NIR absolute PL quantum yield spectrometer (C13534, Hamamatsu Photonics) equipped with an integrating sphere.

## 1.6 Quantum chemical calculations

All of the calculations were carried out with Gaussian 09 program package.[1] Density functional theory (DFT) calculations on the geometrical and electronic properties of the ground-state were performed based on B3LYP[2] density functional method with basis set 6-31G(d, p).[3,4] The density functional dispersion correction was conducted by Grimme’s D3 version with Becke-Johnson damping function.[5] Time-dependent DFT (TD-DFT) calculations were also carried out by this method. Vertical excitation calculations were based on optimized S0 geometries, and geometry optimizations for excited S1 and T1 states were carried out at the same level of theory. The analysis of hole and electron pair distributions was conducted using the Multiwfn code.[6,7] The reorganization energy for S1→S0 and S0→S1 transition were conducted with the Nelson's four-point method.

## 1.7 Analysis of rate constants

The rate constants of radiative decay (kr,S) and nonradiative decay (knr,S) from S1 to S0 states, the rate constants of intersystem crossing (kISC) and reverse intersystem crossing (kRISC) were calculated from the following six equations:

kp=1/τp…………………………………………………………………Eq.(1)

kd=1/τd…………………………………………………………………Eq.(2)

kr,S= Φpkp+Φdkd≈Φpkp…………………………… ………………Eq.(3)

knr,S=1−ΦPLΦPLkr,S…………………………………………………………Eq.(4)

kISC=kp−kr,S−knr,S……………………………….…………………Eq.(5)

kRISC= kpkdΦd/kISCΦp……………………………………………Eq.(6)

Where τp and τd represent the prompt and decay fluorescence lifetime, which determined from transient PL spectra. The kp and kd represent the decay rate constants for prompt and delayed fluorescence, respectively. Φp and Φd indicate prompt and delayed fluorescence components and can be distinguished from the total ΦPL by comparing the integrated intensities of prompt and delayed components in the transient PL spectra.

  - Device Fabrication and Measurement

Before OLEDs fabrication, p-DBFSi, m-DBFSi and m-DBFSi-d were purified by gradient sublimation using a BOF-A-5-60 apparatus (Anhui BEQ Equipment Technology Co., LTD) under a vacuum of 5 × 10⁻5 Pa. To evaluate the EL performance of p-DBFSi, m-DBFSi and m-DBFSi-d as emitter materials, we fabricated multilayered OLEDs. The ITO coated glass substrates with a sheet resistance of 15 Ω square-1 were ultrasonic cleaned with acetone/ethanol and dried with nitrogen gas flow, followed by 20 min ultraviolet light-ozone (UVO) treatment in a UV-ozone surface processor (PL16 series, Sen Lights Corporation). Organic layers were deposited with the rate of 0.2-3 Å s-1 in a high vacuum chamber below 2.0 × 10-5 Pa in an inert gas glovebox. For all the devices, the emitting areas were determined by the overlap of two electrodes as 0.09 cm2. The as-fabricated devices were measured in ambient environment without any encapsulation. The current density-voltage-luminance (J-V-L), EQE-L curves and electroluminescence spectra were collected using a Keithley 2400 source meter and an absolute EQE measurement system (C9920-12, Hamamatsu Photonics, Japan). The device operational lifetime was evaluated by measuring the luminance over time at constant current density.

- Figures and Tables

Figure S1. 1H NMR spectrum of 1 in CDCl3.

Figure S2. 13C NMR spectrum of 1 in CDCl3.

Figure S3. 1H NMR spectrum of 2 in CDCl3.

Figure S4. 13C NMR spectrum of 2 in CDCl3.

Figure S5. 1H NMR spectrum of 3 in CDCl3.

Figure S6. 13C NMR spectrum of 3 in CDCl3.

Figure S7. 1H NMR spectrum of DBFCl in CDCl3.

Figure S8. 13C NMR spectrum of DBFCl in CDCl3.

Figure S9. 1H NMR spectrum of p-DBFSi in CDCl3.

Figure S10. 13C NMR spectrum of p-DBFSi in CDCl3.

Figure S11. HR-MS spectrum of p-DBFSi.

Figure S12. 1H NMR spectrum of m-DBFSi in CDCl3.

Figure S13. 13C NMR spectrum of m-DBFSi in CDCl3.

Figure S14. HR-MS spectrum of m-DBFSi.

Figure S15. 1H NMR spectrum of m-DBFSi-d in CDCl3.

Figure S16. 13C NMR spectrum of m-DBFSi-d in CDCl3.

Figure S17. HR-MS spectrum of m-DBFSi-d.

Figure S18.  1H NMR spectrum of DBFBN in CDCl3.

Figure S19. 13C NMR spectrum of DBFBN in CDCl3.

Figure S20. Single-crystal structure of p-DBFSi (CCDC: 2504406) and m-DBFSi (CCDC: 2504404).

Figure S21. The frontier molecular orbital distributions and energy levels of DBFBN (a), p-DBFSi (b), m-DBFSi (c) and m-DBFSi-d (d).

Figure S22. Fragment-resolved analysis of the S1 excited state for p-DBFSi, m-DBFSi and m-DBFSi-d. (a, b, c) Molecular structures with the fragment partition (Core/Ph/Ph3Si). (d, e, f) S1 hole and electron populations and their overlap resolved on each fragment. (g, h, i) Fragment transition matrix derived from the transition density matrix (TDM) for S1, visualizing intra- and inter-fragment transition intensity. Note: “Core” denotes the MR-active fused BN polycyclic skeleton (green). “Ph” denotes the phenyl ring directly bonded to the MR core (yellow). “Ph3Si” denotes the distal triphenylsilyl periphery beyond the σ-linked Si center (grey).

Figure S23. The reorganization energies (λS0 and λS1) for p-DBFSi (a), m-DBFSi (b) and m-DBFSi-d (c) by the Nelson's four-point method.

Figure S24. The reorganization energies (λS0 and λS1) for p-DBFSi, m-DBFSi and m-DBFSi-d by the Molecular Materials Property Prediction Package (MOMAP).

Figure S25. The Huang–Rhys factors (a) for DBFBN, p-DBFSi, m-DBFSi and m-DBFSi-d by the Molecular Materials Property Prediction Package (MOMAP). (b) Fragment-resolved contributions (core vs periphery) for the dominant vibronic modes, obtained by projecting the normal-mode displacement onto the predefined core atom set to yield a mode-specific core fraction fcore (i) and reporting the HRF-weighted percentage contributions. (c) Core-HRF is defined as Σi HRF(i)× fcore (i), serving as a core-weighted HRF metric that estimates the contribution of MR-core motions to the dominant vibronic coupling. Note: “Core” denotes the fused polycyclic aromatic skeleton excluding TPS and 2,6-dimethylphenyl groups, while “periphery” includes the TPS substituent and the 2,6-dimethylphenyl groups.

Figure S26. The low temperature fluorescence and phosphorescence (measured at 77 K) spectra of p-DBFSi (a), m-DBFSi (b) and m-DBFSi-d (c) in toluene solution.

Figure S27. Photoluminescence (PL) properties of DBFBN and m-DBFSi at different doping concentrations (3, 6 and 9 wt%). Molecular structures of DBFBN (a) and m-DBFSi (b). The fluorescence spectra of DBFBN (c) and m-DBFSi (d) were measured in DMIC-TRZ doped films with different doping concentrations.

Figure S28. Transient photoluminescence decay curves of p-DBFSi (a), m-DBFSi (b) and m-DBFSi-d (c) in doped films.

Figure S29. Temperature-dependent transient PL spectra of p-DBFSi (a), m-DBFSi (b) and m-DBFSi-d (c) in mCBP doped film.

Figure S30. Spin–orbit coupling (SOC) matrix elements between S1 and relevant Tn states of p-DBFSi (a), m-DBFSi (b) and m-DBFSi-d (c).

Figure S31. The horizontal dipole ratio of p-DBFSi (a, d), m-DBFSi (b, e) and m-DBFSi-d (c, f) measured in binary-doped films and ternary-doped films.

Figure S32. The Cyclic voltammetry curves of ferrocene (a), p-DBFSi (b), m-DBFSi (c) and m-DBFSi-d (d).

Figure S33. The TGA curve of p-DBFSi (a), m-DBFSi (b) and m-DBFSi-d (c).

Figure S34. High-performance liquid chromatography (HPLC) chromatograms of p-DBFSi before (a) and after (b) vacuum thermal evaporation.

Figure S35. High-performance liquid chromatography (HPLC) chromatograms of m-DBFSi before (a) and after (b) vacuum thermal evaporation.

Figure S36. High-performance liquid chromatography (HPLC) chromatograms of m-DBFSi-d before (a) and after (b) vacuum thermal evaporation.

Figure S37. The molecular structures of relevant materials employed in devices.

Figure S38. EL spectra of the devices based on (a) p-DBFSi, (b) m-DBFSi and (c) m-DBFSi-d at different voltages.

Figure S39. Current density and luminance versus driving voltage characteristic of the devices based on (a) p-DBFSi, (b) m-DBFSi and (c) m-DBFSi-d.

Figure S40. Electroluminescence (EL) performance of OLEDs based on DBFBN and m-DBFSi at different doping concentrations (3, 6 and 9 wt%). (a, d) The EL spectra of DBFBN- and m-DBFSi-based devices, respectively. (b, e）The EQE-L curves of DBFBN- and m-DBFSi-based devices, respectively. (c, f) The CE-L and PE-L curves of DBFBN- and m-DBFSi-based devices, respectively.

Figure S41. Luminance-deterioration curves of the OLED based on p-DBFSi, m-DBFSi and m-DBFSi-d binary EML system at the initial luminance of 1000 cd m−2.

Figure S42. Electrochemical stability of (a) p-DBFSi, (b) m-DBFSi and (c) m-DBFSi-d (100 cycles).

Figure S43. Fluorescence spectra change of (a) p-DBFSi, (b) m-DBFSi and (c) m-DBFSi-d measured in degassed toluene (1×10-5 M) at room temperature under UV light irradiation. (ΔCIE (x, y) denotes the Euclidean distance on the CIE 1931 chromaticity diagram, i.e., Δ(x,y)=√[(xt−x0)2+(yt−y0)2]).

Figure S44. Absorption spectra of p-DBFSi, m-DBFSi and m-DBFSi-d as well as PL spectrum of Ir(ppy)3 in toluene solution (10-5 M).

Figure S45. OLEDs performances of p-DBFSi, m-DBFSi and m-DBFSi-d based on emitting system that contains p-DBFSi/m-DBFSi/m-DBFSi-d, Ir(ppy)3 sensitizer and DMIC-TRZ host at a concentration ratio of 2: 10: 88. (a) Device structures and energy level diagrams. (b) Electroluminescence spectrum at 1000 cd m−2. (c) EQE-L curve. (d) Current density and luminance versus voltage (J-V-L) characteristics. (e) PE-luminance and CE-luminance curves. (f) Luminance-deterioration curve at the initial luminance (L0) of 5000 cd m−2 (LT(1000 cd m−2) = LT(L₀) × [L₀ / (1000 cd m−2)]n, with an assumed acceleration factor of n = 1.75).[8]

Table S1. Crystal data and structure refinement for p-DBFSi.

| Identification code | p-DBFSi |
| --- | --- |
| Empirical formula | C122H92B2N4O2Si2 |
| Formula weight | 1723.89 |
| Temperature/K | 170.00 |
| Crystal system | triclinic |
| Space group | P-1 |
| a/Å | 15.1378(9) |
| b/Å | 19.3839(11) |
| c/Å | 20.8763(12) |
| α/° | 74.253(2) |
| β/° | 83.299(2) |
| γ/° | 83.612(2) |
| Volume/Å3 | 5835.2(6) |
| Z | 2 |
| ρcalc g/cm3 | 1.272 |
| μ/mm-1 | 2.168 |
| F(000) | 2318.0 |
| Crystal size/mm3 | 0.29 × 0.15 × 0.15 |
| Radiation | GaKα (λ = 1.34139) |
| 2Θ range for data collection/° | 5.132 to 114.542 |
| Index ranges | -18 ≤ h ≤ 18, -24 ≤ k ≤ 24, -26 ≤ l ≤ 24 |
| Reflections collected | 110181 |
| Independent reflections | 23867 [Rint = 0.0800, Rsigma = 0.0742] |
| Data/restraints/parameters | 23867/614/1353 |
| Goodness-of-fit on F2 | 1.114 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0700, wR2 = 0.2144 |
| Final R indexes [all data] | R1 = 0.0926, wR2 = 0.2334 |
| Largest diff. peak/hole / e Å-3 | 1.09/-0.37 |

Table S2. Crystal data and structure refinement for m-DBFSi.

| Identification code | m-DBFSi |
| --- | --- |
| Empirical formula | C64H46B2N6 |
| Formula weight | C122H92B2N4O2Si2 |
| Temperature/K | 1723.89 |
| Crystal system | triclinic |
| Space group | P-1 |
| a/Å | 15.9961(18) |
| b/Å | 25.868(3) |
| c/Å | 26.700(3) |
| α/° | 65.080(5) |
| β/° | 88.639(5) |
| γ/° | 89.909(5) |
| Volume/Å3 | 10016(2) |
| Z | 4 |
| ρcalc g/cm3 | 1.256 |
| μ/mm-1 | 1.167 |
| F(000) | 3960.0 |
| Crystal size/mm3 | 0.16 × 0.11 × 0.04 |
| Radiation | GaKα (λ = 1.34139) |
| 2Θ range for data collection/° | 4.808 to 97.804 |
| Index ranges | -17 ≤ h ≤ 17, -25 ≤ k ≤ 29, -29 ≤ l ≤ 29 |
| Reflections collected | 90292 |
| Independent reflections | 29582 [Rint = 0.1383, Rsigma = 0.1903] |
| Data/restraints/parameters | 29582/30/2393 |
| Goodness-of-fit on F2 | 1.353 |
| Final R indexes [I>=2σ (I)] | R1 = 0.1623, wR2 = 0.3981 |
| Final R indexes [all data] | R1 = 0.2132, wR2 = 0.4316 |
| Largest diff. peak/hole / e Å-3 | 1.39/-0.54 |

Table S3. Quantitative fragment-resolved localization of frontier molecular orbitals (HOMO and LUMO) for p-DBFSi, m-DBFSi and m-DBFSi-d.

| Emitter | HOMO% (core) | HOMO% (Ph) | HOMO% (Ph3Si) | LUMO% (core) | LUMO% (Ph) | LUMO% (Ph3Si) |
| --- | --- | --- | --- | --- | --- | --- |
| p-DBFSi | 99.571 | 0.395 | 0.022 | 89.331 | 9.448 | 1.215 |
| m-DBFSi | 99.587 | 0.038 | 0.023 | 90.741 | 8.810 | 0.443 |
| m-DBFSi-d | 99.587 | 0.038 | 0.023 | 90.741 | 8.809 | 0.443 |

Note: “Core” denotes the MR-active fused BN polycyclic skeleton (green). “Ph” denotes the phenyl ring directly bonded to the MR core (yellow). “Ph3Si” denotes the distal triphenylsilyl periphery beyond the σ-linked Si center (grey).

Table S4. Summary of reported green MR-TADF materials with FWHM ≤ 25 nm in dilute toluene.

| Emitter | λPL [nm] | FWHMPL [nm] | Ref. |
| --- | --- | --- | --- |
| p-DBFSi | 517 | 15 | This work |
| m-DBFSi | 515 | 14 |  |
| m-DBFSi-d | 515 | 14 |  |
| BN-ICz-1 | 521 | 21 | Angew. Chem. Int. Ed. 2022, 61, e202202380. |
| BN-ICz-2 | 521 | 22 |  |
| v-DABNA-CN-Me | 496 | 17 | Adv. Mater. 2022, 34, 2201778. |
| DtCzBTPTRZ | 521 | 24 | CCS Chem. 2022, 4, 2065. |
| DBNO | 500 | 19 | Angew. Chem. Int. Ed. 2022, 61, e202200337 |
| tCzphB-Ph | 523 | 21 | Nat. Commun. 2022, 13, 4876. |
| tCzphB-Fl | 531 | 21 |  |
| ω-DABNA | 509 | 22 | J. Am. Chem. Soc. 2023, 145, 1505. |
| DBNT-2 | 512 | 20 | Nat. Photonics 2023, 17, 280. |
| 2PyBN | 499 | 21 | Chem. Sci.,2023, 14, 3326. |
| IDID2BN | 524 | 25 | Angew. Chem. Int. Ed. 2023, 62, e202313254. |
| DBF-DBN | 514 | 22 | Chem. Commun., 2023, 59, 5126. |
| DBT-DBN | 516 | 19 |  |
| BO-DICz | 507 | 18 | Angew. Chem. Int. Ed. 2023, e202318742. |
| TPABO-DICz | 515 | 17 |  |
| 6z | 516 | 22 | Angew. Chem. Int. Ed. 2024, 63, e202402020. |
| BNBO | 500 | 25 | Molecules 2024, 29, 841. |
| BpIC-DPA | 527 | 25 | Chem. Eng. J. 2024, 481, 148781. |
| ω-DABNA-M a | 514 | 23 | Nat. Commun. 2024 15, 3174. |
| SS-DAO | 512 | 21 | Angew. Chem. Int. Ed. 2024, 63, e202316710. |
| BpIC-DPA | 527 | 25 | Chem. Eng. J. 2024, 481, 148781. |
| BpIC-Cz | 534 | 22 |  |
| BN-2Pm | 505 | 20 | Chem. Eur. J. 2025, 31, e202404484. |
| ω’-DABNA | 513 | 19 | Angew. Chem. Int. Ed. 2025, 64, e202512162. |
| ω’-DABNA-D | 513 | 19 |  |
| QB-DPA | 495 | 15 | Angew. Chem. Int. Ed. 2025, 64, e202418348. |
| QB-PXZ | 508 | 15 |  |
| CNBN | 501 | 14 | Angew. Chem. Int. Ed. 2025,64, e202500108. |
| MCNBN | 510 | 15 |  |
| PCNBN | 503 | 18 |  |
| PMCNBN | 512 | 19 |  |
| DBNDS-TPh | 517 | 16 | Adv. Mater. 2025, 37, 2416224. |
| DBNDS-DFPh | 518 | 16.6 |  |
| DBNDS-CNPh | 518 | 16.4 |  |
| DBSe-BN | 514 | 21 | Adv. Mater. 2025, e13987. |
| DBNDO-1 | 512 | 14.8 | Angew. Chem. Int. Ed. 2025, e202515889. |
| DBNDO-2 | 517 | 14.1 |  |
| DBNDO-3 | 518 | 16.2 |  |
| tBN-NPTrz | 527 | 24 | Chem. Eng. J. 2025, 507, 160656. |
| tBN-DNPTrz | 529 | 22 |  |

a Measured in a PMMA film

Table S5. Summary of thermal and electrochemical data.

| Emitter | Td [oC] | HOMO [eV] | LUMO [eV] |
| --- | --- | --- | --- |
| p-DBFSi | 516 | −5.13 | −2.75 |
| m-DBFSi | 505 | −5.12 | −2.72 |
| m-DBFSi-d | 513 | −5.10 | −2.71 |

Table S6. Summary of rate constants in 3 wt% DMIC-TRZ-doped films.

| Emitter | kr,S [a] [107 s-1] | knr,S b [105 s-1] | kISC c [108 s-1] | kRISC d [105 s-1] |
| --- | --- | --- | --- | --- |
| p-DBFSi | 2.2 | 8.9 | 1.2 | 1.6 |
| m-DBFSi | 3.6 | 3.8 | 1.2 | 1.1 |
| m-DBFSi-d | 3.8 | 3.7 | 1.3 | 1.2 |

The rate constants of [a] radiative decay (kr,S), [b] non-radiative decay (knr,S), [c] intersystem crossing (kISC), [d] reverse intersystem crossing (kRISC).

Table S7. Summary of reported OLED performances in bottom-emitting based on green MR-TADF with CIEy ≥ 0.65. Note: binary-EML and ternary-EML OLEDs were shown in white and green background, respectively.

| Emitters | λEL [nm] | FWHM [nm] | CIE [x, y] | EQEmax [%] | CEmax [lm W−1] | PEmax [lm W−1] | Operational Lifetime | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| diboron skeleton |  |  |  |  |  |  |  |  |
| p-DBFSi | 520 | 19 | 0.18, 0.74 | 37.2 | 140.7 | 165.4 | LT50 = 299 h @1000 cd m−2 | This work |
|  | 521 | 20 | 0.19, 0.74 | 34.2 | 127.2 | 156.1 | LT80 = 85 h @5000 cd m−2 |  |
| m-DBFSi | 517 | 17 | 0.15, 0.76 | 40.1 | 143.2 | 187.5 | LT50 = 371 h @1000 cd m−2 |  |
|  | 518 | 18 | 0.18, 0.75 | 37.7 | 134.3 | 175.9 | LT80 = 120 h @5000 cd m−2 |  |
| m-DBFSi-d | 517 | 17 | 0.14, 0.76 | 41.9 | 146.7 | 191.8 | LT50 = 450 h @1000 cd m−2 |  |
|  | 518 | 18 | 0.17, 0.75 | 38.6 | 137.6 | 184.9 | LT80 = 149 h @5000 cd m−2 |  |
| DBTN-2 | 520 | 29 | 0.19, 0.74 | 35.2 | 132.9 | 130.4 | - | Nat. Photonics. 2023, 17, 280. |
| DBF-DBN | 521 | 31 | 0.22, 0.71 | 21.5 | - | 76.2 | - | Chem. Commun. 2023, 59, 5126. |
| DBT-DBN | 520 | 24 | 0.22, 0.70 | 31.3 | - | 93.6 | - |  |
| IDID2BN | 534 | 29 | 0.31, 0.65 | 36.6 | 146.3 | 135.2 | - | Angew. Chem. Int. Ed. 2023, 62, e202313254. |
| DBNDS-TPh | 524.6 | 19.3 | 0.17, 0.75 | 35.2 | 139.0 | - | LT50 < 1 h @ 5000 cd m-2 | Adv. Mater. 2025, 37, 2416224. |
|  | 524.6 | 19.6 | 0.20, 0.74 | 37.5 | 139.0 | - | LT50 ≈ 12 h @ 5000 cd m-2 |  |
| DBNDS-DFPh | 523.0 | 19.8 | 0.17, 0.76 | 34.5 | 136.0 | - | LT50 < 1 h @ 5000 cd m-2 |  |
|  | 523.0 | 20.3 | 0.19, 0.75 | 35.5 | 133.7 | - | LT50 ≈ 10 h @ 5000 cd m-2 |  |
| DBNDS-CNPh | 521.5 | 19.3 | 0.17, 0.75 | 29.8 | 113.0 | - | LT50 < 1 h @ 5000 cd m-2 |  |
|  | 523.0 | 20.5 | 0.19, 0.74 | 32.3 | 116.5 | - | LT50 ≈ 11 h @ 5000 cd m-2 |  |
| DBNDO-1 | 518.4 | 19 | 0.14, 0.75 | 31.1 | 113.9 | - | LT50 = 0.34 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2025, e202515889. |
| DBNDO-2 | 520.7 | 19 | 0.16, 0.75 | 32.4 | 119.6 | - | LT50 = 0.43 h @ 1000 cd m-2 |  |
| DBNDO-3 | 524.4 | 19 | 0.18, 0.75 | 32.0 | 123.3 | - | LT50 = 0.53 h @ 1000 cd m-2 |  |
| CNBN | 506 | 16 | 0.12, 0.68 | 34.4 | 98.3 | 128.7 | - | Angew. Chem. Int. Ed. 2025, 64, e202500108. |
| MCNBN | 517 | 17 | 0.17, 0.74 | 30.8 | 111.4 | 145.8 | - |  |
| PCNBN | 508 | 20 | 0.14, 0.67 | 29.1 | 85.2 | 95.6 | - |  |
| PMCNBN | 519 | 22 | 0.19, 0.73 | 27.2 | 99.6 | 111.8 | - |  |
| multiboron skeleton (n ≥ 3, n is the number of B atoms) |  |  |  |  |  |  |  |  |
| ω-DABNA | 512 | 25 | 0.13, 0.73 | 31.1 | 101.0 | 98.1 | LT95 = 25 h @ 1000 cd m-2 LT80 = 292 h @ 1000 cd m-2 | J. Am. Chem. Soc. 2023, 145, 1505. |
| ω-DABNA-M | 515 | 25 | 0.15, 0.74 | 32.7 | - | 114.5 | LT95 = 24 h @ 1000 cd m-2 | Nat. Commun. 2024 15, 3174. |
|  | 517 | 23 | 0.17, 0.70 | 28.2 | - | 98.7 | LT95 = 110 h @ 1000 cd m-2 |  |
|  | 517 | 26 | 0.27, 0.66 | 19.1 | - | 67.3 | LT95 = 63 h @ 1000 cd m-2 |  |
| ω-DABNA-PH | 521 | 30 | 0.19, 0.74 | 31.8 | - | 27.4 | LT95 = 27 h @ 1000 cd m-2 |  |
|  | 522 | 29 | 0.21, 0.69 | 26.5 | - | 98.6 | LT95 = 109 h @ 1000 cd m-2 |  |
|  | 522 | 30 | 0.24, 0.70 | 24.4 | - | 107.5 | LT95 = 580 h @ 1000 cd m-2 |  |
| ω'-DABNA | 517 | 25 | 0.16, 0.73 | 32.3 | 118.0 | 154.5 | LT80 = 188 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2025, 64, e202512162. |
|  | 518 | 26 | 0.21, 0.77 | 33.4 | 122.2 | 143.9 | LT80 = 236 h @ 5000 cd m-2 |  |
| ω'-DABNA-D | 519 | 25 | 0.16, 0.75 | 34.6 | 128.5 | 155.5 | LT80 = 321 h @ 1000 cd m-2 |  |
|  | 519 | 26 | 0.20, 0.72 | 32.6 | 120.4 | 132.1 | LT80 = 394 h @ 5000 cd m-2 |  |
| QB-PXZ | 516 | 20 | 0.18, 0.74 | 36.6 | 134.8 | 151.3 | LT80 = 485 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2025, 64, e202418348. |
| monoboron skeleton |  |  |  |  |  |  |  |  |
| m-Cz-BNCz | 520 | 44 | 0.24, 0.69 | 27.4 | 102.2 | 107.1 | - | Angew. Chem. Int. Ed. 2020, 59, 17442. |
| AZA-BN | 527 | 30 | 0.27, 0.69 | 28.2 | - | 121.7 | LT90 = 46.3 h @ 2000 cd m-2 | Angew. Chem. Int. Ed. 2020, 59, 17499. |
| BBCz-G | 515 | 54 | 0.26, 0.68 | 31.8 | - | - | - | J. Am. Chem. Soc. 2020, 142, 19468. |
| PXZ-BN | 516 | 47 | 0.22, 0.67 | 23.3 | 83.8 | 70.1 | - | J. Mater. Chem. C 2021, 9, 8308. |
| TCz-B | 515 | 30 | 0.16, 0.71 | 29.2 | 100.7 | 72.4 | LT50 = 2.0 h @ 100 cd m-2 | Angew. Chem. Int. Ed. 2021, 60, 23142. |
| 2PTZBN | 528 | 58 | 0.28, 0.65 | 25.5 | 96.5 | 86.6 | - | Chem. Eng. J. 2021, 426, 131169. |
| v-DABNA-CN-Me | 504 | 23 | 0.13, 0.65 | 31.9 | 88.9 | 93.6 | - | Adv. Mater. 2022, 34, 2201778. |
| DBNO | 512 | 41 | 0.22, 0.67 | 33.1 | 114.4 | 115.9 | - | Angew. Chem. Int. Ed. 2022, 61, e202200337. |
| helicene-BN | 523 | 49 | 0.26, 0.66 | 31.5 | 117.5 | 153.8 | - | CCS Chem. 2022, 4, 3463. |
| BNSSe | 515 | 50 | 0.22, 0.66 | 35.7 | 124.2 | 156.2 | LT50 = 4.8 h @ 1000 cd m-2 | Nat. Photonics. 2022, 16, 803. |
| BNSeSe | 512 | 48 | 0.19, 0.66 | 36.8 | 121.0 | 146.3 | LT50 = 4.1 h @ 1000 cd m-2 |  |
| tCzphB-Ph | 527 | 24 | 0.21, 0.75 | 29.3 | - | - | - | Nat. Commun. 2022, 13, 4876. |
|  | 526 | 27 | 0.21, 0.74 | 31.3 | - | - | LT90 = 0.5 h @ 23300 cd m-2 |  |
| tCzphB-Fl | 535 | 26 | 0.26, 0.72 | 26.2 | - | - | - |  |
|  | - | - | 0.26, 0.71 | 29.7 | - | - | LT90 = 12.4 h @ 24500 cd m-2 |  |
| TCz-VTCzBN | 524 | 37 | 0.22, 0.71 | 32.2 | 96.7 | 129.3 | - | Angew. Chem. Int. Ed. 2022, 61, e202209984. |
| DtCzB-TPTRZ | 520 | 41 | 0.23, 0.68 | 30.6 | 105.8 | 116.2 | - | CCS Chem. 2022, 4, 2065. |
| BN-ICz-1 | 523 | 23 | 0.22, 0.74 | 20.5 | - | 84.2 | LT90 = 82.3 h @ 2000 cd m-2 | Angew. Chem. Int. Ed. 2022, 61, e202202380. |
| BN-ICz-2 | 52 | 23 | 0.23, 0.73 | 29.8 | - | 102.9 | LT90 = 71.3 h @ 2000 cd m-2 |  |
| TRZCzPh-BNCz | 513 | 37 | 0.17, 0.68 | 32.5 | - | 101.4 | LT50 = 13.4 h @ 500 cd m-2 | Angew. Chem. Int. Ed. 2022, 61, e202210210. |
| TRZTPh-BNCz | 513 | 33 | 0.16, 0.70 | 31.4 | - | 99.5 | LT50 = 14.7 h @ 500 cd m-2 |  |
| BN-TP | 528 | 36 | 0.26, 0.70 | 35.1 | 139.3 | 139.3 | LT50 = 28.8 h @ 4000 cd m-2 | Angew. Chem. Int. Ed. 2022, 61, e202204652. |
| BN-TP-N1 | 532 | 34 | 0.28, 0.69 | 34.9 | 137.7 | 139.7 | - | Angew. Chem. Int. Ed. 2023, 62, e202301930. |
|  | 532 | 34 | 0.30， 0.67 | 33.2 | 130.3 | 139.1 | - |  |
| BN-TP-N2 | 534 | 36 | 0.30, 0.67 | 31.9 | 129.5 | 139.8 | - |  |
|  | 534 | 35 | 0.30, 0.67 | 31.3 | 126.5 | 142.0 | - |  |
| BN-TP-N3 | 524 | 33 | 0.23, 0.71 | 37.3 | 135.5 | 139.9 | - |  |
|  | 524 | 34 | 0.26, 0.69 | 35.4 | 129.8 | 139.9 | - |  |
| BN-TP-N4 | 528 | 35 | 0.27, 0.70 | 36.5 | 136.3 | 143.2 | - |  |
|  | 528 | 36 | 0.28, 0.69 | 32.7 | 130.0 | 143.4 | - |  |
| BN-Py | 532 | 37 | 0.29, 0.68 | 30.6 | 119.6 | 118.9 | - | Adv. Mater. 2023, 35, 2305125. |
|  | 532 | 38 | 0.29, 0.68 | 31.0 | 110.6 | 110.1 | - |  |
| 2PyBN | 505 | 26 | 0.12, 0.65 | 37.1 | 106.7 | 139.6 | - | Chem. Sci., 2023, 14, 3326. |
| BN-STO | 517 | 34 | 0.19, 0.70 | 40.1 | 141.2 | 176.9 | LT50 = 35 h @ 1000 cd m-2 | Angew. Chem. Int. Ed. 2023, 62, e202302478. |
| BN-XTO | 516 | 34 | 0.19, 0.70 | 37.3 | 131.0 | 156.9 | LT50 = 354 h @ 1000 cd m-2 |  |
| TPABO-DICz | 522 | 22 | 0.24, 0.74 | 25.8 | 84.1 | 100.5 | - | Angew. Chem. Int. Ed. 2043, 63, e202318742. |
| BNDCN | 507 | 30 | 0.13, 0.65 | 32.3 | 104.3 | 76.2 | - | Chem. Commun. 2024, 60, 574. |
| BNBO | 508 | 36 | 0.17, 0.65 | 24.3 | - | 62.2 | - | Molecules 2024, 29, 841. |
| h-BNCO-1 | 528 | 39 | 0.24, 0.71 | 40.1 | - | 147.0 | LT95 = 140 h @ 1000 cd m-2 | Nat. Commun. 2024, 15, 731. |
|  | 525 | 39 | 0.23, 0.71 | 25.1 | - | - | LT95 = 46 h @ 1000 cd m-2 | Nat. Commun. 2024, 15, 4394. |
|  | 529 | 39 | 0.26, 0.70 | 24.9 | - | - | LT95 = 124 h @ 1000 cd m-2 |  |
|  | 530 | 39 | 0.26, 0.68 | 16.3 | - | - | LT95 = 322 h @ 1000 cd m-2 |  |
|  | 530 | 39 | 0.27, 0.69 | 17.9 | - | - | LT95 = 437 h @ 1000 cd m-2 |  |
| tCzBN-PQ | 524 | 37 | 0.25, 0.67 | 30.2 | 115.6 | 94.3 | - | Chem. Eng. J. 2024, 481, 148794. |
| tCzBN-PQCz | 517 | 38 | 0.20, 0.69 | 35.1 | 131.0 | 106.9 | - |  |
| BThPAc-1 | 516 | 34 | 0.18, 0.72 | 24.8 | 87.9 | 98.7 | - | Chem. Sci. 2024, 15, 13290. |
| BThPAc-2 | 514 | 33 | 0.17, 0.72 | 25.8 | 89.9 | 106.8 | - |  |
| DCz-SFBN | 506 | 37 | 0.15, 0.65 | 29.2 | - | 89.7 | - | Mater. Horiz. 2024, 11, 4674. |
| DPhCz-SFBN | 522 | 37 | 0.22, 0.70 | 31.0 | - | 122.2 | - |  |
|  | 520 | 37 | 0.23, 0.69 | 31.1 | - | 140.9 | - |  |
| CzTCz-SFBN | 518 | 35 | 0.20, 0.71 | 28.1 | - | 103.0 | - |  |
|  | 521 | 37 | 0.22, 0.68 | 26.2 | - | 110.7 | - |  |
| 3CzSF-BN | 522 | 36 | 0.21, 0.72 | 20.3 | 76.2 | 88.7 | - | Adv. Optical Mater. 2024, 12, 2400490. |
|  | 519 | 37 | 0.20, 0.71 | 23.1 | 82.9 | 66.8 | - |  |
| Th-BN | 516 | 41 | 0.23, 0.68 | 34.6 | 122.9 | 134.3 | - | Chem. Sci. 2024, 15, 11435. |
| SBNO | 524 | 40 | 0.26, 0.68 | 25.7 | 86.4 | 71.4 | - | Small 2024, 20, 2407220. |
| SBNOS | 522 | 40 | 0.25, 0.69 | 32.7 | 99.7 | 80.3 | - |  |
| BpIC-DPA | 536 | 29 | 0.30, 0.67 | 22.0 | 94.0 | 98.8 | LT90 = 156.1 h @ 1000 cd m-2 | Chem. Eng. J. 2024, 481, 148781. |
| m-ICz-BNCz | 516 | 40 | 0.20, 0.70 | 28.0 | - | 81.9 | - | Adv. Optical Mater. 2024, 12, 2400200. |
| dm-ICz-BNCz | 534 | 46 | 0.30, 0.67 | 32.9 | - | 105.8 | - |  |
| Spiro-BNCz | 533 | 48 | 0.29, 0.67 | 34.2 | 140.5 | 90.1 | - | Aggregate. 2024, 5, e445. |
| TCzBAO | 520 | 36 | 0.20, 0.70 | 25.1 | 90.5 | 101.5 | - | Adv. Optical Mater. 2024, 12, 2301711. |
| 6z | 513 | 27 | 0.18, 0.70 | 31.7 | 109.2 | 122.6 | - | Angew. Chem. Int. Ed. 2024, 63, e202402020. |
|  | 515 | 36 | 0.28, 0.65 | 27.0 | 92.5 | 73.6 | - |  |
| 2SBN | 514 | 45 | 0.20, 0.65 | 27.1 | 74.90 | 71.48 | - | Adv. Optical Mater. 2024, 12, 2401754. |
| 3SBN | 514 | 43 | 0.20, 0.66 | 27.0 | 90.3 | 55.6 | - |  |
| MesPXZ-tCzBN | 528 | 54 | 0.31, 0.65 | 27.6 | 110.6 | 150.3 | - | Adv. Optical Mater. 2024, 13, 2402131. |
| BN-2Pm | 514 | 27 | 0.17, 0.71 | 32.8 | 92.3 | 76.3 | - | Chem. Eur. J. 2025, 31, e202404484. |
| DBSe-BN | 517 | 24 | 0.18, 0.73 | 38.8 | 139.3 | 156.3 | LT50 = 1341 h @ 1000 cd m-2 | Adv. Mater. 2025, e13987. |
|  | 518 | 25 | 0.22, 0.71 | 33.4 | 123.4 | 136.1 | LT50 = 318 h @ 5000 cd m-2 |  |
| m-PAz-BNCz | 528 | 37 | 0.26, 0.70 | 36.2 | 132.1 | 133.9 | - | Adv. Mater. 2025, 37, 2503383. |
|  | 528 | 39 | 0.28, 0.68 | 35.7 | 135.3 | 152.1 | - |  |
| m-SFAz-BNCz | 532 | 38 | 0.28, 0.69 | 33.7 | 129.1 | 128.1 | - |  |
|  | 532 | 40 | 0.30, 0.67 | 31.2 | 123.8 | 143.1 | - |  |
| m-DPAcPAz-BNCz | 524 | 37 | 0.24, 0.70 | 33.8 | 129.0 | 135.1 | - |  |
|  | 524 | 40 | 0.27, 0.68 | 33.8 | 124.2 | 143.6 | - |  |
| m-TPAz-BNCz | 532 | 38 | 0.28, 0.69 | 33.9 | 125.2 | 131.1 | - |  |
|  | 532 | 40 | 0.29, 0.67 | 32.2 | 121.7 | 139.9 | - |  |
| tBN-DNPTrz | 532 | 36 | 0.29, 0.67 | 29.3 | 103.8 | - | LT95 = 360 h @ 5000 cd m-2 | Chem. Eng. J. 2025, 507, 160656. |

Table S8. Bond dissociation energy (BDE) of the CPAH−CTPS bonds (red) or CPAH−Si (blue) bonds of the emitters optimized at the B3LYP/6-31G (d, p) level.

| Emitter | CPAH−CTPS [eV] | CPAH−Si [eV] |
| --- | --- | --- |
| p-DBFSi | 4.771 | 3.843 |
| m-DBFSi | 4.784 | 3.850 |
| m-DBFSi-d | 4.802 | 3.886 |

Table S9. Bond dissociation energy (BDE) of the C−N bonds and C−B bonds of the emitters optimized at the B3LYP/6-31G (d, p) level.

| Bond | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DBFBN (BDE, eV) | 4.572 | 4.321 | 4.228 | 4.848 | 4.510 | 4.565 | 4.832 |
| m-DBFSi (BDE, eV) | 4.570 | 4.498 | 4.232 | 4.847 | 4.510 | 4.573 | 4.839 |

Table S10. Summary of EL characteristics of OLEDs based on DBFBN and m-DBFSi at different doping concentrations.

| Emitter | Von [a] [V] | λEL [b] [nm] | FWHM [b] [nm] | Lmax [c] [cd m−2] | CEmax [d] [cd A−1] | PEmax [e] [lm W−1] | EQE [f] [%] | CIE [b] (x, y) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 wt % DBFBN | 2.4 | 510 | 17 | 84893 | 103.3 | 125.5 | 34.3 | (0.11, 0.72) |
| 6 wt % DBFBN | 2.4 | 511 | 18 | 63718 | 96.3 | 116.3 | 29.7 | (0.12, 0.73) |
| 9 wt % DBFBN | 2.4 | 513 | 20 | 50209 | 81.3 | 98.2 | 25.9 | (0.14, 0.73) |
| 3 wt % m-DBFSi | 2.4 | 517 | 17 | 83364 | 143.2 | 187.5 | 40.1 | (0.15, 0.76) |
| 6 wt % m-DBFSi | 2.4 | 517 | 17 | 82220 | 138.3 | 169.3 | 38.8 | (0.15, 0.76) |
| 9 wt % m-DBFSi | 2.4 | 517 | 17 | 83421 | 132.6 | 160.2 | 37.2 | (0.15, 0.75) |

[a] Turn-on voltage recorded at the luminance of 1 cd m−2; [b] Recorded at 1000 cd m-2; [c] Maximum brightness; [d] Maximum current efficiency; [e] Maximum power efficiency; [f] Maximum EQE.

Table S11. Statistical summary of EL characteristics of binary OLEDs based on p-DBFSi, m-DBFSi and m-DBFSi-d

| Emitter | Von [a] [V] | λEL[b] [nm] | FWHM [b] [nm] | CEmax [d] [cd A−1] (average) | PEmax [e] [lm W−1] (average) | EQE [f] [%] (average) |
| --- | --- | --- | --- | --- | --- | --- |
| p-DBFSi | 2.4 | 520 | 19 | 140.7 (134.7±3.0) | 165.4 (157.1±4.6) | 37.2 (36.3±0.6) |
| m-DBFSi | 2.4 | 517 | 17 | 143.2 (141.6±0.9) | 187.5 (180.9±5.3) | 40.1 (39.7±0.3) |
| m-DBFSi-d | 2.4 | 517 | 17 | 146.7 (145.2±1.7) | 191.8 (185.1±4.5) | 41.9 (41.0±0.7) |

[a] Turn-on voltage recorded at the luminance of 1 cd m−2; [b] Recorded at 1000 cd m-2; [c] Maximum current efficiency; [d] Maximum power efficiency; [e] Maximum EQE. All the average values in the parentheses are based on the measurement from ten independent devices.

- References

- M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria, M. A. Robb, J. R. Cheeseman, G. Scalmani, V. Barone, G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. Marenich, J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian, J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, D. Williams-Young, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. A. Montgomery, Jr., J. E. Peralta, F. Ogliaro, M. Bearpark, J. J. Heyd, E. Brothers, K. N. Kudin, V. N. Staroverov, T. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi, J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, and D. J. Fox, Gaussian, Inc., Wallingford CT, 2016.

- A. D. Becke, J. Chem. Phys. 1993, 98, 5648.

- P. C. Hariharan, J. A. Pople, Theoret. Chim. Acta, 1973, 28, 213.

- R. Ditchfield, W. J. Hehre, J. A. Pople, J. Chem. Phys. 1971, 54, 724.

- L. Goerigk, A. Hansen, C. Bauer, S. Ehrlich, A. Najibi, S. Grimme, Phys. Chem. Chem. Phys. 2017, 19, 32184.

- T. Lu, F. Chen, J. Comput. Chem. 2012, 33, 580.

- Z. Liu, T. Lu, Q. Chen, Carbon 2020, 165, 461.

- X. Cai, Y. Xu, Y. Pan, L. Li, Y. Pu, X. Zhuang, C. Li, Y. Wang, Angew. Chem. Int. Ed. 2023, 62, e202216473.