## Slide 1
Junho Kim
(e-mail : junho.kim@uni-koeln.de / jhk4733@gmail.com)
Displays without image distortion - Hybrid Auxetic Metamaterial Platforms
Kim, S.-B.†, Kim, J.† et al., Nature Communications 17, 7389 (2026) · doi:10.1038/s41467-026-74141-6 († equal contribution)

## Slide 2
Flat
Flexible (2013~)
Curved (2013)
Stretchable
Foldable (2019~)
Rollable (2020~)
Display form factor
Product images: manufacturers' press materials

## Slide 3
Stretchable display

## Slide 4
Stretchable electronics applications
Wearable / Skin display
Soft robotics
Bioelectronics
Interactive surface
IEEE Spectrum, vol. 58, no. 6, pp. 38-43, June 2021

## Slide 5
Introduction
PDMS
Substrate of stretchable electronics
Ecoflex
Rubber | 0.5 | PET | 0.43
PDMS | 0.45~0.5 | Glass | 0.18~0.3
Gold | 0.42 | Foam | 0.1~0.5
Copper | 0.33 | Ice | 0.33
Poisson’s ratio
y
x
eaxial
etrans
Poisson’s ratio (n)
Poisson’s ratio of material
SEBS

## Slide 6
[1]
[4]
[3]
[2]
[1] A kirigami-inspired island-chain design for wearable moistureproof perovskite solar cells with high stretchability and performance stability†
[3] 3D-Printed Liquid Metal Interconnects for Stretchable Electronics
[4] Highly stretchableelectroluminescent skin for opticalsignaling and tactile sensing
[2] Shi, Xiang, et al. "A self-healing and stretchable light-emitting device." Journal of Materials Chemistry C 6.47 (2018): 12774-12780.
[5] Muth, J.T.; Vogt, D.M.; Truby, R.L.; Mengüç, Y.; Kolesky, D.B.;Wood, R.J.; Lewis, J.A. Embedded 3D printing of strain sensors
within highly stretchable elastomers. Adv. Mater. 2014, 26, 6307–6312. [CrossRef] [PubMed]
Research issues in stretchable displays
[5]
Using intrinsically stretchable materials as a substrate, image distortion is unavoidable.
Although a LED with a stretchable auxetic structure was implemented, substrate selection options were limited and the distortion-free area was restricted.

## Slide 7
Utilization of auxetic structures
Auxetics are structures for materials that have a negative Poisson’s ratio. When stretched, they become thicker perpendicular to the applied force
Extrem. Mech. Lett. 2017, 12, 77–85
Various auxetic structures
q
q +dq
l
dx
dy
(ideal, rigid theory)
Re-entrant type, honeycomb
Chiral type, tetrachiral
Rotating unit type, square
from wikimedia
Mechanical characteristics of rotating square unit
Adv. Funct. Mater. 2022, 32 (22), 2113299.
Nano Energy 2021, 89 (Part B), 106447.

## Slide 8
Recent research & limitations
Promising, but distortion-free behavior is limited to the centers of the rotating squares — the rest of the substrate is still distorted.
Even an ideal ν = 0 does not preserve the aspect ratio — the stretched axis still elongates the image by (1+ε); only ν = −1 preserves it.
In practice the Poisson's ratio is not exactly zero, and local non-uniformity induces additional image distortion inside the substrate.
Nat Commun 15, 7146 (2024)
Adv. Funct. Mater. 2024, 34, 2406725
Auxetic substrate with Poisson’s ratio of -1
Bidirectional auxetic substrate with Poisson’s ratio of 0

## Slide 9
Limitations of rotating square based auxetic structures
Von Mises Stress (N/m2)
Polymers (Basel). 2019, 11 (6).
Nano Energy 2021, 89 (Part B), 106447.
: Detector area
Uniaxial strain applied to rotating square unit
Fhandle
F’handle
F”handle
The handles suppress the rotation of nearby squares: rotation is reduced near the handles and only gradually recovers toward the interior — spatial uniformity is inherently limited.
Aactive
Atotal
Aactive/Atotal ~12%
To prevent image distortion in LED applications, it's crucial to ensure not only a simple strain uniformity but also an effective area where uniformity is maintained.

## Slide 10
Isotropic expansion
The rotation-based unit-cell kinematics are not locally isotropic — even when the outer boundary exhibits ν = −1, interior points expand anisotropically. Gripping parts add further non-uniformity, addressed separately in the framework optimization.

## Slide 11
Hybrid auxetic metamaterial platform
Optimized auxetic framework
Defining optimized connection points

## Slide 12
Simulation model of auxetic framework
Tracing points (a, b)
Stretching-driven component
Two tracing points a, b are placed where the k-value (k = u·r/|r|²) is most affected by the grips. For each uniaxial stretching direction (horizontal / vertical), Δk_ab(ε) = |k_a − k_b| is evaluated over ε = 0–15%, and the geometry (W, L, D) is chosen to minimize S = max(Γ_H, Γ_V). [Nat. Commun. 17, 7389, Eq. 2–3]

## Slide 13
(i) Best case / (ii) Worst case
Optimization of the auxetic frameworks

## Slide 14
Uniform auxetic effect — best case (i) vs worst case (ii)

## Slide 15
Determination of adhesive point position
Point displacement vector
Ideally, the point displacement vector for each adhesive point ) should be proportional to its position vector ). Which can be expressed as,
Position vector
: Proportional constant)
Here, is constant for every adhesive point. This means that strain uniformity can be achieved if the A points are stretched at the same rate, regardless of their distance from the origin.
Displacement vector for uniform strain
For practical use, the value of must be sufficiently small (e.g. ~ 10 deg). Then, by calculating a set of that satisfy the condition, isotropic expansion can be implemented for stretching along both the x- and y-axes (diagonal: extension beyond the published paper).
For pratical use (handle)

## Slide 16
Defining a position of adhesive point in matrix region
Binary spatial distribution: M(x,y)
Spatial distribution matrix : N(x,y)
km,n = Mm,nNm,n
k1,1 = M1,1N1,1, k1,2 = M1,2N1,2
 Region at x-y space
0
0.25
0.12
: Angular separation between and
Published notation: Mᵢⱼ = 𝟏[α < 10°], Nᵢⱼ = u·r/|r|, Kᵢⱼ = MᵢⱼNᵢⱼ — paper evaluates Kᴴ at ε = 3% (worst case, H) and Kᵛ at ε = 15%.

## Slide 17
Defining the adhesion point using our fundamental basis
Possible zone for adhesive point sets
0.25
0.12
, where
1 cm
Center
1
2
3
4
5
6
7
y-direction
x-direction
, at the same position are superposed into a single map using both data sets, and the common valid region is identified as candidate anchor sites.
x
y
z
●
Published pipeline: Kᴴ at ε = 3%, Kᵛ at ε = 15% → superposition → 10% tolerance (next slide).
Notes: 같은 위치에서 3개의 값은 다른 데이터로 구분되어 합쳐져야 하고, 합쳐진 결과는 가시적으로 보여져야 한다.

## Slide 18
Optimized connection points

## Slide 19
Isotropic expansion factor

## Slide 20
Digital image correlation (DIC) analysis
FEA vs DIC: u = k·r realized — isotropic expansion with ρ ≈ 0.99
DIC matches FEA: on the proposed platform |u| grows linearly with |r| in all directions (u = k·r), unlike the fully bonded case. Right (Fig. 4b): isotropic expansion factor ρ ≈ 0.99 for the proposed platform vs ≈ 0.95 fully bonded, consistently over ε = 3–15%.

## Slide 21
DIC measurement
Conventional scheme (Fully bonded)
Tensile property measurements
Tensile strain
Proposed scheme
Initial state (e=0%)
Initial state (e=0%)
Stretched (e=15%)
Stretched (e=15%)
Image distortion analysis

## Slide 22
LED demo: distortion-free operation under stretching
Initial state (ε = 0%, emission)
Stretched (e = 18%)
Initial state (ε = 0%, ambient)
10 × 8 array
10 × 10 array
Extended demonstration beyond the published paper (paper: 7 × 5 array and 10 × 10 passive-matrix array, ε up to 15–20%; <2% luminance drop after 500 stretch cycles at 15%).

## Slide 23
Summary
1
Stretchable is the first form factor in which the screen area itself grows
Image distortion becomes a first-order problem: an elastomer (ν ≈ +0.5) skews the aspect ratio by ~1.24× at 15% strain — and a global ν = −1 alone does not guarantee local isotropy (rotation-based kinematics, gripping effects).
2
Hybrid auxetic platform: grip-aware framework design + selective bonding
Optimize the framework with the grips inside the objective, S(W, L, D) = max(Γ_H, Γ_V) → W/D ≈ 35; then bond the continuous elastomer only where u = k·r holds (superposed Kᴴ/Kᵛ maps, 10% tolerance).
3
Isotropic expansion factor ρ quantifies image distortion field-wide
ρ = Cov(R, U)/σ_R·σ_U; the proposed platform sustains ρ ≈ 0.99 (DIC, ε = 3–15%) vs ≈ 0.95 fully bonded, and LED arrays operate distortion-free up to 20% strain.
Kim, S.-B., Kim, J. et al. Hybrid auxetic metamaterial platforms enabling multiscale isotropic expansion for distortion-free stretchable displays. Nat. Commun. 17, 7389 (2026).

## Slide 24
Thank you

## Slide 25
Experimental steps : Rotating square auxetic framework
Fabrication process
Auxetic framework geometry
1. SAM treatment on 3D-printed mold
2. Pouring of Dragon-skin10 onto the mold
3. Delamination of Dragon-skin soft mold
4. SAM treatment on Dragon-skin soft mold
5. Pouring of Smooth-cast 61D onto the Dragon-skin soft mold
6. Scraping out the residual Smooth-cast to form flat surface
7. Delamination of Dragon-skin soft mold
8. Free standing auxetic frameworks
Soft mold
Master mold
Rotating square
Scraper

## Slide 26
Experimental steps : Band/Substrate/Adhesive
Form-preserving component fabrication
1. Pouring of Dragon-skin onto petri dish
2. Degassing & curing at RT overnight
3. Cutting through Band-shape mold
4. Delamination of band from the petri dish
4. Delamination of band-substrate structure
3. After curing at RT overnight, cutting the outside of the band
2. Putting the band onto the surface of uncured substrate
1. Spin-coating of substrate material
Band
Band-substrate structure
4. Alignment of band-substrate structure onto the uncured silcone adhesive
3. Scraping the residual adhesive & lifting the metal mask
2. Coating of silicone adhesive onto the hole of the metal mask
1. Alignment of FP-coated metal mask onto the auxetic framework
Silicone adhesive masking
FP-coated metal mask
Silicone adhesive

## Slide 27
Simulation results analyzed by algorithm (D variation)
0.86
0.48
0.67
L (mm)
W (mm)
L (mm)
W (mm)
L (mm)
W (mm)
L (mm)
W (mm)
1.6
0.8
1.2
2.4
1.6
1.2
3.0
2.4
2.8
D = 0.4 mm
D = 0.8 mm
D = 0.6 mm
D = 1.0 mm

## Slide 28
Simulation results analyzed by algorithm (L variation)
2.88
0.47
1.7
D(mm)
W (mm)
D (mm)
W (mm)
D (mm)
W (mm)
D (mm)
W (mm)
2.96
0.51
1.74
3.03
0.55
1.79
3.07
0.59
1.83
L = 0.4 mm
L = 0.8 mm
L = 0.6 mm
L = 1.0 mm

## Slide 29
Mechanically engineered adhesive position
Strain distribution (Fixed point)
x
y
z
●
x
y
Adhesive point engineering (Biaxial strain)
eaxial
etrans
eaxial
etrans
n at (0,0,0)
w/o fixed points
w/o fixed points
n at (0,0,0)
eaxial = 20%
eaxial =etrans, y = 20%
To obtain a Poisson's ratio of -1, an adhesive point should be perpendicular to its symmetric point. (qFP = 0)
qFP
x
y
|e | (%)
0
400
300
200
100
2 mm

## Slide 30
Initial concept: Strain transfer by low Young’s modulus substrate
Elastomer (E=5kPa) (e.g. Silbione)
Rotating square type auxetic struture (E=110MPa) (e.g. Smooth-cast 61D)
Would it be possible to minimize the suppression of the torque of the rotating square if there is a significant difference in Young's modulus?
In-plane displacement
x
y
z
●
0
16 mm
12
8
4
( )
2 cm
Poisson’s ratio(n ) ~ 1
Auxetic + Elastomer
Elastomer only
Exaggerated by 300% in the z-axis direction
Assuming that Young's modulus of the substrate is very low, if the substrate is attached to the entire surface of the square island, it acts as a fixed point and inhibits rotation.
However, due to its uneven stretching from the origin, image distortion cannot be avoided.

## Slide 31
Flow chart for simulation & experiment
Single elastomer (Fixed points/ Biaxial strain by )
Parameter optimization of auxtic structures in all directional stretching
Integration of simulation sets & determination of the adhesive position sets
Parameter optimization for entire structure in all directional stretching
Fabrication of auxetic framework
Material selection / mold design
Parameter measurement
Fabrication of band/substrate structure
Alignment of adhesive point
Adhesive force test for silicone adhesive & each interface
Mold design